## Slide 1
Atomistic Solution Models
Consider a system with N interacting particles and a number of energy states numbered with the j index
Partition Function
A = -kBT ln(Z)
Energy states will be degenerate, that is more than one state can have the same energy, then,
Relative to T = 0K

## Slide 2
Ideal Solution Model
Sterling’s Approximation

## Slide 3
Ideal Solution Model

## Slide 4
Regular Solution Model
Coordination number ”z” z = 6 for Cartesian Coordinates
NAA = number of A-A contacts with an energy of uAA
Lattice has N sites
Total number of pairs is zN/2
Average energy of pure A is UA = zNAuAA/2
For A atoms there are zNA pairwise interactions made up of 2 interactions for each A and one for each AB

## Slide 5
Regular Solution Model

## Slide 6
Regular Solution Model
µA ~ dG/dxA

## Slide 9
Entropy of Mixing
A) Here we consider a combinatorial entropy of mixing and a binary enthalpy of mixing
B) A change in organization can also occur which leads to an additional entropic term
=
Where , a critical temperature
Tf = DHf/DSf

## Slide 10
Vibrational Contribution
With vibrational part
ZA is vibrational partition function of A
U’ is internal energy minus vibrational part
G = H –TS so last term is the non-configurational (non-combinatorial) entropic terms
GA=NAlnZA = lnZANA
Hildebrandt type parameter for vibrational contributions

## Slide 11
Excess molar Gibbs energy of mixing for quasi-regular solution
G = H –TS so first term is enthalpic, second is entropic
t is a characteristic temperature, when T = t ideal solution behavior is seen

## Slide 12
T = t Ideal
T > t Mix
T < t Demix
For Positive W
T = t Ideal
T > t Demix
T < t Mix
For Negative W
For W = 0
Ideal

## Slide 13
T = t Ideal
T > t Mix
T < t Demix
For Positive W
T = t Ideal
T > t Demix
T < t Mix
For Negative W
For W = 0
Ideal
~ W/kT
~A + B/T
A positive B positive Demix
A negative B negative Mix
A negative B positive UCST
A positive B negative LCST

## Slide 14
Mean Field (what we have considered) Interactions are random, there is no structuring
Specific Interactions Interactions are not random, there is identity between interacting pairs
Coulombic Interaction for instance

## Slide 15
Correlations
Dilute: Ideal behavior, there are no interactions
Semi-dilute: weak or strong interactions are possible
With weak interactions the system can be treated with a “mean field”. No correlation is observed, we can use the second virial coefficient and Hildebrand Model
With strong interactions we need to use detailed information about interactions, correlation function or other models

## Slide 16
Virial Coefficient Approach for Weak Interactions (Mean Field)
Consider that two materials mix, A is matrix and B is diluent
B behaves like an ideal gas in A when B is dilute
P = rRT
The presence of B creates a pressure called an osmotic pressure P
This pressure can be measured for particles in a solution such as proteins in water
At higher concentrations with a mean-field we can use a virial expansion to describe the pressure
= rRT(1 + A2 r + A3 r2 + A4 r3 + …) Where A2 is the second virial coefficient and reflects binary interactions in a mean field
By comparison with the Van der Waals equation of state where v = 1/r
A2 = b – a/RT where “b” is the “excluded volume” and “a” is the attractive interaction potential for B’s
P/r = energy ~ rRT A2 = r(RT b – a)

## Slide 17
Virial Coefficient Approach for Weak Interactions (Mean Field)
P/r = energy ~ rRT A2 = r(RT b – a)
Dilute: Ideal behavior, there are no interactions
Semi-Dilute
A2 = 0 Ideal/critical point
A2 > 0 Miscible
A2 < 0 Immiscible
T = a/(bR) Ideal
T < a/bT Miscible
T > a/bT Immiscible
Dilute: Ideal behavior, there are no interactions
Semi-dilute
W = 0 Ideal
< 0 Miscible
> 0 Immiscible
T = t Ideal
T > t Miscible
T < t Immiscible

## Slide 18
A. How to deal with more than (h(r) or g(r)) binary interactions c(r)
Correlation Function, h(r)
A recursive relationship.
Requires a closure relationship to find a solution.
Closure relationships: Random Phase Approximation (RPA) r => 0
Percus-Yevick Approximation (complex)
Born-Green Approximation (simpler)

## Slide 19
Strong Interactions (Specific Interactions)
Correlation Function, h(r)
A recursive relationship.
Requires a closure relationship to find a solution.
Fourier transform of the OZ function; a convolution becomes a product.
Fourier Transform of a structural correlation function is the scattered intensity which is composed of a form factor F2(q) and a structure factor S(q). If we measure a dilute system with no correlations I0(q) and if
I(q) = S(q) F2(q) = S(q) I0(q) (f/f0)
We can assume a model for c(k) and calculate S(q) = I(q)/I0(q) (f0/f) Structure factor (the peak part of scattering)

## Slide 20
Correlations
Dilute: Ideal behavior, there are no interactions
Semi-dilute: weak or strong interactions are possible
With weak interactions the system can be treated with a “mean field”. No correlation is observed, we can use the second virial coefficient and Hildebrand Model
With strong interactions we need to use detailed information about interactions, correlation function or other models

## Slide 21
Strong Interactions (Specific Interactions)
Correlation Function, h(r)
A recursive relationship.
Requires a closure relationship to find a solution.
Percus-Yevick Approximation Closure.
Binary RDF = Total RDF - RDF with no binary interaction
Use a function then
Use this in the OZ equation yields the RDF with no binary interactions
g(r) = h(r)
g(r) or h(r)
https://www.chemeurope.com/en/encyclopedia/Percus-Yevick_approximation.html
Binary correlation
Correlation fun. without direct interactions

## Slide 22
B. How to deal with more than binary interactions
BBGKY hierarchy (Bogoliubov-Born-Green-Kirkwood-Yvon)
Probability density function in position, qi, and momentum, pi, per particle
Liouville Equation
Force acting on particle ”i”
Integrate the Liouville Equation yields a chain of equations relating binary interactions with ternary interactions; ternary interactions with quaternary interactions etc. This cannot be solved unless a model is used for fs+1.

## Slide 23
Strong Interactions (Specific Interactions)
Correlation Function, h(r)
A recursive relationship.
Requires a closure relationship to find a solution.
Closure relationships: Random Phase Approximation (RPA) r => 0
Percus-Yevick Approximation; Born-Green Approximation
g(r) = h(r)
For a square well potential: A2
P = rRT(1 + A2 r + A3 r2 + A4 r3 + …)

## Slide 24
Strong Interactions

## Slide 25
S(q) = f0I(q)/(fI0(q)) Structure factor

## Slide 26
Strong Interactions
Center Atom
Side Atom
Body Diagonal Atom
Face Diagonal Atom

## Slide 27
Strong Interactions

## Slide 28
Weak Interactions
Strong Interactions
I(q,f) = I(q,f0) S(q,f) f/f0
A2 ~ n

## Slide 29
There are many models, the book mentions the Quasi-Chemical Model which is used in Calphad and ThermoCalc
Elliot and Lira give a reasonable discussion of various models in Chapters 7, 11, 12
Chapter 7
Van der Waals: Includes excluded volume, ”b”, and attractive interaction “a”
Peng-Robinson: Attractive interaction term is more complicated and includes the acentric factor w. ”a” has a temperature dependence.
These equations have a cubic form:
Models for Interactions Based on a Mean Field Approach

## Slide 30
Hard core model for Van der Waals
Z = PV/RT = 1/(1-br) – (a/RT) r
Compare with Molecular Dynamics (o) for Hard Spheres E&W
Hard core no attractive interaction, hP = br

## Slide 31
Margulis one-parameter Model
Chapter 11 Elliot and Lira
Hildebrand Model
Margulis acid-base Model

## Slide 32
Redlich-Kister Model (asymmetric phase diagrams)
Two-parameter Margulis Model

## Slide 33
Van der Waals Models
Regular Solution Models
-SUV
H A
-pGT
G = H – ST
H = U + PV
So
G = U + PV – TS
(A = U – TS)
Ignore PV which is small G ~ A
If V ~ S ~ 0 then G = U
This is a regular solution
Van Laar Model
For Symmetric Mean-Field Models there are two main problems, organizational entropy change on mixing and changes in volume on mixing
Consider 11, 22, and 12 interactions
Consider Lattice sites do not have the same volume, V1, V2

## Slide 34
Van Laar Model
Include asymmetry

## Slide 35
Scatchard-Hildebrand Theory
Theory based on Volume Fraction rather than Mole Fraction
d = Solubility Parameter
Volume Fraction
Cohesive Energy Density
U = H – PV

## Slide 37
Scatchard-Hildebrand Theory

## Slide 38
Scatchard-Hildebrand with Adjustable Parameter

## Slide 39
Flory-Huggins Model for Polymers
Point Masses have no volume
Real molecules have excluded volume
Only the available volume can be used to mix so the entropy of mixing should be modified
w accounts for the available volume

## Slide 40
Flory-Huggins Model for Polymers
r = V2/V1 2 is polymer

## Slide 41
Account for Hydrogen Bonding
MOSCED Model (MOdified Separation of Cohesive Energy Density)
Calculates the infinite dilution activity coefficient
This is used in another model to fit parameters at infinite dilution to the MOSCED model
Such as Redlich-Kister, van Laar, or below
li dispersion factor
ti is the polarity
qi is .9 to 1

## Slide 42
Account for Hydrogen Bonding
SSCED Model (Simplified Separation of Cohesive Energy Density)

## Slide 43
Local Clustering Models

## Slide 44
For Pure components
Local Clustering Models

## Slide 45
To obtain Helmholz Free energy use
Need an expression for W as a function of temperature
Local Clustering Models

## Slide 47
Wilson’s Equation
Temperature dependence of W
Two activation energies 1 around 2 and 2 around 1
Assume G ~ A (PV is insignificant)
Break G into a residual (energetic) contribution that vanishes at T => ∞ and a combinatorial (size and shape) contribution
Temperature dependence of W

## Slide 48
Two activation energies 1 around 2 and 2 around 1
Assume G ~ A (PV is insignificant)
Break G into a residual (energetic) contribution that vanishes at T => ∞ and a combinatorial (size and shape) contribution
Use Flory’s expression for the combinatorial contribution
Wilson’s Equation
Temperature dependence of W

## Slide 49
Wilson’s Equation
Temperature dependence of W

## Slide 50
Non-Random Two Liquid Model (NRTL)
G = U + PV –ST if you ignore PV and ST and say G ~ U then an integration isn’t needed

## Slide 51
Universal Quasi-Chemical Model (UNIQUAC)
Temperature dependence of W depends on surface area rather than volume
Interactions occur at surfaces qi ~ surface area of component ”i”
Surface Area Fraction
Last term accounts for non-spherical surface area effects on mixing (branched chains)

## Slide 52
Guggenheim Modification to Universal Quasi-Chemical Model (UNIQUAC)
r is volume ratio, q is surface area ratio
Both obtained from group contribution method

## Slide 54
Universal Functional Activity Coefficient Model (UNIFAC)
Combinatorial term same as UNIQUAC (surface area based)
Residual term involves group contribution rather than whole molecule

## Slide 55
Solutions with multiple sub-lattices
NaCl-KBr or Spinels AB2O4
Cation sublattice
Anion sublattice
Octahedral sublattice
Tetrahedral sublattice
Disorder in the placement of Na+ and K+
And Cl- and Br- leads to entropy

## Slide 56
Solutions with multiple sub-lattices
Ideal Solution Model (Temkin Model)
Cations surrounded by anions in crystal and in the melt
Quasi-lattice approach
Random mixing of cations and anions on their respective sub-lattices
Consider a system AC and BC

## Slide 57
Solutions with multiple sub-lattices
Regular Solution Model (Temkin Model)
Need to account for next nearest neighbor interactions since nearest neighbor interactions do not change, that is Na+ Cl- interactions, you need Na+ K+ interactions
There are ½ zN nearest neighbor as well as next nearest neighbor interactions
Same as for regular solution

## Slide 58
Solutions with multiple sub-lattices
Same as for regular solution

## Slide 59
Order-disorder systems
s = Order parameter a number that goes from 0 for disordered to 1 for ordered
Convergent ordering occurs when two lattice sites are equivalent in the disordered state and crystallographically distinct in the ordered state
This occurs in solid solutions
Bragg and Williams
Solution of A and B with lattice sites a and b
AB forms at low temperatures A at a sites is ½ (1 + s)
NA + NB = 2N zN interactions
Disordered State
Regular Solution
s = Order parameter
Bragg and Williams

## Slide 60
Order-disorder systems
Disordered State
Regular Solution
Ideal Solution
H = U + PV
Bragg and Williams

## Slide 61
Second Order Transition
Bragg and Williams

## Slide 62
Order-disorder systems
Non-Convergent ordering occurs when two lattice sites are distinct in the disordered state and distinct in the ordered state
Spinels: One tetrahedral and two octahedral cations AB2O4
A can be in tetrahedral or octahedral sites
Normal Spinel x = 0
Inverse Spinel x = 1
Random Spinel x = 2/3
S = 0 for x = 0 Regular Spinel
Bragg and Williams

## Slide 63
Ordered and Regular Spinels disorder at high temperature to increase entropy

## Slide 64
For a Normal Spinel the disordering process is:

## Slide 65
Mass-action law treatment of defect equilibria
Perovskite type oxide
Non-stoichiometric Compounds
Three sublattices
A 12 coordination
B 6 coordination number
O
A open circles 12
Black B 6
Grey O
O and vacancies on the O lattice randomly arranged
B atoms are reduced by oxygen vacancies

## Slide 66
Solid Solution Approach
Non-stoichiometric Compounds
Sum over all vibrational states “s”
Over all configurations “c”
Configurations with degeneracy gc and Gibbs energy of formation DfGc
Proposition: A perovskite ABO3-d is made up of ABO3 and ABO2.5 in an ideal solution (no defect defect interactions)