## Slide 1
Course Summary
I. Introduction
II. Single component systems
III. Solutions
IV. Phase diagrams
V. Phase stability
VI. Surfaces
VII. Heat of formation
VIII. Heat capacity
IX. Solution models and equations of state
X. Thermodynamics and materials modeling
XI. Experimental methods

## Slide 2
I. Introduction:
Define Terms;
Basic Definitions;
Gibbs Thompson;
Hess’ Law (not path dependent);
Second law and reversibility;
Equilibrium;
Third law T = 0 K Boltzmann equation;
Legendre transform;
Maxwell equations;
Gibbs-Duhem equation (Gibbs phase rule)
Course Summary

## Slide 3
What happens to the energy when I heat a material?
Or How much heat, dq, is required to change the temperature dT? (Heat Capacity, C)
dq = C dT
C = dq/dT
Constant Volume, CV
Constant Pressure, Cp
dU = dq + dw
With only pV work (expansion/contraction), dwec = -pdV
dU = dq – pdV
For constant volume
(dU)V = dq, so
CV = (dU/dT)V, or the energy change with T: (dU)V = CV dT
dU = dq + dw = dq – pdV (only e/c work, i.e. no shaft work)
Invent Entropy H = U + PV so dH = dU + pdV + Vdp
(dH)p = dU + pdV for constant pressure
With only pV work (expansion/contraction), dwec = -pdV
dq = dU + pdV = (dH)p
Cp = (dH/dT)p , or the enthalpy change with T: (dH)p = Cp dT
Constant Volume
Computer Simulation
Helmholtz Free Energy, A
A = U – TS = G - pV
Constant Pressure
Atmospheric Experiments
Gibbs Free Energy, G
G = H – TS = A + pV
-S U V
H A
-P G T

## Slide 4
Size dependent enthalpy of melting
(Gibbs-Thompson Equation)
For bulk materials, r = ∞, at the melting point DG = DH – T∞DS = 0
So, T∞ = DH/DS Larger bonding enthalpy leads to higher T∞ , Greater randomness gain on melting leads to lower T∞.
For nanoparticles there is also a surface term,
(DG) V = (DH – TrDS)V + sA = 0, where Tr is the melting point for size r nanoparticle
If V = r3 and A = r2 and using DS = DH/T∞ this becomes,
r = s/(DH(1– Tr/T∞)) or Tr = T∞ (1 - s/(rDH)
Smaller particles have a lower melting point, and the dependence suggests a plot of Tr/T∞ against 1/r
-S U V
H A
-P G T

## Slide 5
Derive the expression for Cp – CV
Cp - Cv = a2VT/kT
a = (1/V) (dV/dT)p
kT = (1/V) (dV/dP)T
CV = (dU/dT)V
From the Thermodynamic Square
dU = TdS – pdV so CV = (dU/dT)V = T (dS/dT)V - p (dV/dT)V
Second term is 0 dV at constant V is 0
(dS/dT)V = CV /T
Similarly
Cp = (dH/dT)p
From the Thermodynamic Square
dH = TdS + Vdp so Cp = (dH/dT)p = T (dS/dT)p - V (dp/dT)p
Second term is 0 dp at constant p is 0
(dS/dT)p = Cp /T
Write a differential expression for dS as a function of T and V
dS = (dS/dT)VdT + (dS/dV)TdV using expression for CV above and Maxwell for (dS/dV)T
dS = CV /T dT + (dp/dT)VdV use chain rule: (dp/dT)V = -(dV/dT)p (dP/dV)T = Va / (VkT)
Take the derivative for Cp: Cp/T = (dS/dT)p = CV /T (dT/dT)p + (a/kT)(dV/dT)p = CV /T + (Va2/kT)
Cp - Cv = a2VT/kT
-S U V
H A
-p G T

## Slide 6
Gibbs-Duhem Equation
Consider a binary system A + B makes a solution
At constant T and p:
Fundamental equation with chemical potential:
So, at constant T and p:
Reintroducing the T and p dependences:
Intensive properties are not independent, T, p, µ
For I components, only I – 1 have independent properties (Gibbs phase rule) if T and p are variable.
Determine partial molar quantities at equilibrium from number of moles
Partial vapor pressure from total vapor pressure
-S U V
H A
-p G T

## Slide 7
Clausius-Clapeyron Equation
Consider two phases at equilibrium, a and b
dma = dmb
-S U V
H A
-p G T
dG = Vdp –SdT
so
Vadp – SadT = Vbdp – SbdT
so
dptrans/dT = DS/DV
and
DG = 0 = DH – TtransDS so DS = DH/Ttrans
and
dptrans/dT = DH/(TtransDV) Clapeyron Equation
For transition to a gas phase, DV ~ Vgas
and for low density gas (ideal) V = RT/p
d(lnpvap)/dT = DHvap/(RTvap2) Clausius-Clapeyron Equation
This allows calculation of the vapor pressure as a function of T

## Slide 8
Course Summary
II. Single Component Systems:
First order transition;
Clausius-Clapeyron equation (vapor pressure calculation);
Second order transition;
Virial equation of state for phase diagram;
Phase diagram P vs T (Gibbs phase rule)
Fugacity;
Van der Waals equation (Cubic equation of state);
CALPHAD and PREOS programs

## Slide 9
Clausius-Clapeyron Equation
d(ln pSat)/dT = DHvap/(RTvap2) Clausius-Clapeyron Equation
d(ln pSat) = (-DHvap/R) d(1/T) So, plot ln pSat vs 1/T
ln[pSat/ pCSat] = (-DHvap/R) [1/T – 1/TC] Use the critical point as the reference state
Shortcut Vapor Pressure Calculation:

## Slide 10
Like the Van’t Hoff Equation for Reaction Equilibria so escape of an ideal gas from liquid state is like a chemical reaction equilibria
Consider a chemical reaction with equilibrium constant Keq
dma = dmb
DG = DH – TDS
DG = -RTlnKeq
So lnKeq = -DH/RT + DS/R
Take derivative relative to T
d(ln Keq) = DH/RT2 dT Van’t Hoff Equation
Can determine DH from the mole fraction of reactants and products
-S U V
H A
-p G T
So, plot ln Keq vs 1/T

## Slide 11
Clausius Clapeyron Equation
d(ln pSat) = (-DHvap/R) d(1/T)
ln[pSat/ pRSat] = (-DHvap/R) [1/T – 1/TR]
This is similar to the Arrhenius Plot

## Slide 12
What About a Second Order Transition?
For Example: Glass Transition Tg versus P?
There is only one “phase” present. A flowing phase and a “locked-in” phase for Tg.
There is no discontinuity in H, S, V
dV = 0 = (dV/dT)p dT + (dV/dp)T dp = VadT – VkTdp
dp/dTg = Da/DkT
Tg should be linear in pressure.
a = (1/V) (dV/dT)p
kT = (1/V) (dV/dP)T

## Slide 13
Second order transition Neel Temperature (like Curie Temp for antiferromagnetic)
Inden Model t = T/Ttr
For t <1

## Slide 14
Single Component Phase Diagrams
For a single component, an equation of state relates the variables of the system, PVT
Isochoric phase diagram

## Slide 15
Gibbs Phase Rule

## Slide 16
P= RT/V
Cubic Equation of State
Cubic Equation of State
Solve cubic equations (3 roots)
Ideal Gas Equation of State
Van der Waals Equation of State
Virial Equation of State
Peng-Robinson Equation of State (PREOS)
Z = 1
Law of corresponding states
P = RTr/(1-br) – a r2

## Slide 18
Landau theory for 2’nd order transitions
The order parameter G could be concentration (normal phase separation), magnetization (magnets) , orientation (LCs)
The point is to find a value for G above and below the critical point Tc (where phase separation become possible).
Particularly above Tc, G = 0 and we have no ”order” (think of no magnetization above the Curie temperature or no deviation from the average composition (r - < r >) above the critical temperature).
-The free energy is analytic (there is a function in G and T)
-The free energy F is symmetric in G (only even powers of G)
For simplicity, take a two term Taylor series expansion DF = a(T) G 2 + b(T)/2 G 4
Near the critical temperature assume for simplicity
DF = a0 (Tc - T) G 2 + b0/2 G 4
For a solution to G, you must have b0 > 0 (this is obvious below); and a(T) must change sign for phase separation to occur at Tc so a(T) = a0 (Tc - T)
At the critical point ∂F/∂G = 0 = 2a0 (Tc - T) G0 + 2b0 G03
To minimize free energy and make a stable phase either G0 = 0 (above Tc) or G02 = - a0 (Tc - T)/b0 (for T ≤ Tc)
For T ≤ Tc, G0 ~ (Tc - T)1/2 The critical exponent is ½ for Landau theory.
G
G0
G

## Slide 19
Course Summary
III. Solutions:
Ideal mixing;
Real solutions;
Activity and activity coefficient;
Excess Gibbs free energy;
Raoult’s Law and Henry’s Law;
Hildebrand Model;
Hildebrand del parameter;
Asymmetric models (Redlich-Kister Expression);
Gibbs-Duhem for Solutions;

## Slide 20
An “Ideal Solution” means:
The change on mixing:
DS = -nkB (xA ln(xA) + xB ln(xB))
Since (ln x) is always negative or 0, DS is always positive for ideal solutions
DG = -T DS
Since (ln x) is always negative or 0, DG is always negative (or 0) and ideal solutions always mix
DH is 0, there is no interaction in ideal mixtures, there is no excluded volume, particles are ghosts to each other
DV = (dDG/dp)T = 0, there is no loss or gain of volume compared to the summed volume

## Slide 21
Real Solutions
xA becomes aA the activity so
DGmixing = RT(xAlnaA + xAlnaB)
Excess DGmixing = DGmixing - RT(xAlnxA + xBlnxB)
= RT(xAln(aA/xA) + xBln(aB/xB) )
= RT(xAln(gA) + xBln(gB))
g Is the activity coefficient
Excess DSmixing = -R(xAln(gA) + xBln(gB))
Method to use departure functions for calculations (PREOS.xls)
Calculation of properties in the ideal state is simple
With an equation of state, the departure function can be calculated
For any transition first calculate the departure function to the ideal state
Then carry out the desired change as an ideal mixture or gas
Then use the departure function to return to the real state

## Slide 22
Hildebrand Regular Solution Model
The change on mixing:
DS = -nkB (xA ln(xA) + xB ln(xB)) Ideal Solution
Since (ln x) is always negative or 0, DS is always positive for ideal solutions
DG = DH -T DS
Since (ln x) is always negative or 0, DG is positive or negative depending on DH :: can mix or demix
Depending on the sign of DH
DV = (dDG/dp)T = 0, there is no loss or gain of volume compared to the summed volume
DH = n W xAxB
is the interaction coefficient or regular solution constant
Molar Gibbs free energy of mixing
DGm = RT(xA ln(xA) + xB ln(xB)) + W xAxB
W = zNA[uAB – (uAA+uBB)/2]
The equation is symmetric

## Slide 23
Asymmetric equations for asymmetric phase diagram
Sub-regular solution model
Redlich-Kister Expression

## Slide 24
Use of the Gibbs-Duhem Equation to determine the activity of a component
Constant p, T
If you know gA you can obtain gB by integration
Restatement of Gibbs-Duhem for Solutions

## Slide 25
Course Summary
IV. Phase Diagrams:
Eutectic;
Solid Solution;
L/V vs S/L Ideal; Azeotrope/Congruent; Heteroazeotrope/Eutectic;
Regular solution model;
Lower critical solution behavior (LCST);
Freezing point depression;
Ternary phase diagram;

## Slide 26
Phase Diagrams
Gibbs Phase Rule
Eutectic Phase Diagram Ag + Cu
Univariant Equilibrium
Liquidus
Solidus
Invariant Equilibrium
Eutectic
Lever Rule
Tieline (conode)
and
Silver acts like a solvent to copper and copper acts like a solvent to silver with limited solubility that is a function of temperature with a solubility limit at the eutectic point (3 phases in equilibrium)
L => a + B

## Slide 27
Solve for xBSS xBliq since xA + xB =1
Ideal
Cp(T) is constant
Calculate the Phase Diagram for a Solid Solution

## Slide 28
Solid solution is flatter than ideal (Pos. deviation or destabilized) Liquid is deeper than ideal (Neg. Deviation or stabilized)
Deviations are associated with minima in phase diagram

## Slide 29
Azeotrope
Heteroazeotrope
Liquid/Vapor Equilibria
Ideal
Solid/Liquid Equilibria
Ideal
Eutectic
Non-Ideal
Congruent melting solid solution
Phase diagram is split into two phase diagrams with a special composition that acts as a pure component
Same crystallographic structure in solid solution phase
Different crystallographic structures in solid solution phases
L => a
L => a + b
L => a + L

## Slide 30
Two Different Crystallographic
Phases at Equilibrium
One Crystallographic
Phase
g => a + b

## Slide 31
Polyvinylmethyl Ether/Polystyrene (LCST Phase behavior)
DGm = RT(xA ln(xA) + xB ln(xB)) + W xAxB
must have a temperature dependence for UCST
W = A + B/T so that it gets smaller with increasing temperature this is a non-combinatorial entropy i.e. ordering on mixing
2-Phase
Single Phase
2-Phase
Single Phase

## Slide 32
Freezing Point Depression
dµB,Solid = VmB,Solid dP – SmB,Solid dT + RT d(lnaB,Solid)
Pure solid in equilibrium with a binary solution following Henry’s Law
Isobaric, pure component B so lnaB,Solid = 0
dµB,Solid = – SmB,Solid dTfp
Binary solution following Henry’s Law
dµB,Solution = – SmB,Solultion dTfp + RTfp d(lnyB,Solution)P,T
For small x: e-x = 1 - x + … or ln(1-x) = -x
So, for small yB,Solution: lnyB,Solution ~ -yA,Solution
So,
SmB,Solid dTfp = SmB,Solution dTfp + RTfp dyA,Solution
dyA,Solution = (SmB,Solid - SmB,Solution)/(RTfp) dTfp ~ -DSmB/(RTfp) dTfp = -DHmB/(RTF) (dTfp)/Tfp
yA,Solution = -DHmB/(RTF) ln(Tfp/TF) For small x: ln(x) = x – 1
yA,Solution = -DHmB/(RTF) (Tfp/TF - 1) = -DHmB/(RT2F) DT
Tfp = TF - yA,SolutionRT2F/DHmB

## Slide 33
Course Summary
V. Phase Stability:
Metastable;
Supercool; superheat; supersaturate;
Kauzmann Paradox;
Thermal/density fluctuations;
Spinodal decomposition;
Binodal; spinodal; critical conditions;
Polymorphs; allotrophs;

## Slide 34
The book considers first a reversible chemical reaction A <=> B
Cyclohexane from boat to chair conformation for instance
As temperature changes you can observer a different mix of states, E = kBT ~ 2.5 kJ/mole at RT
But fluctuations allow for 0.1 % boat conformation. At 1073K 30% boat. Probability is exp(-E/kT).
The percent in boat can be measured using NMR spectroscopy.
Chair
Chair
Boat
Transition
State
Metastable
Transition
State
The equilibrium point depends on temperature, kBT

## Slide 35
Superheating and Melting
Superheating can occur since melting occurs at surfaces and if the surfaces are stabilized then superheated solids can be produced
Growth of a liquid phase relies on growth of a mechanical instability
A mechanical instability will not spontaneously grow if it occurs in a meta-stable region in T and P:
(dG/dx)=0 defines equilibrium or binodal; (d2G/dx2) = 0 defines the metastable limit or spinodal
(d3G/dx3) = 0 defines the critical point
G = -ST + Vp, dG = -SdT + Vdp
(d2G/dp2)T = (dV/dp)T < 0 and (d2G/dT2)p = -(dS/dT)p < 0
First requires that the bulk modulus be positive,
Second requires positive heat capacity, (dS/dT)p = Cp/T > 0
Shear modulus goes to 0 at highest possible supercritical solid
-S U V
H A
-p G T

## Slide 36
Kauzmann Paradox,
a thermodynamic basis for the glass transition
The entropy of the liquid becomes smaller than the entropy of the solid at the Kauzmann temperature, TK. This could be the infinite cooling glass transition temperature.

## Slide 37
Since cN depends on 1/T specifying cN specifies the temperature. Large cN is low tempearature.

## Slide 38
Polymorphs and Allotrophs
Allotroph: Carbon as diamond or graphite
Polymorph: Titania as anatase or rutile
Silica as α-quartz, β-quartz, tridymite, cristobalite, moganite, coesite, and stishovite
Calcium carbonate as calcite or argonite
Ostwald step rule: Least stable polymorph crystallizes first since it has
a free energy that is closest to the liquid or solution state. This means that metastable phases form kinetically first if they exist. If many polymorphs exist, they will form in order of free energy with the highest forming first.
Ostwald’s rule: Most stable polymorph does not always crystallize, rather, meta-stable polymorphs form at a higher rate if the surface tension difference between the melt/liquid solution and the polylmorph is small.
Ostwald ripening: Metastable polymorphs may form small crystals. Over time stable polymorphs grow from these small crystals into large crystals. This has been generalized to growth of large phases due to ripening such as in crushed ice or ice cream.
Ostwald Freundlich Equation: Small crystals dissolve more easily than large crystals. This is the reason for Ostwald ripening. Also true for vapor pressure of a liquid droplet (replace x with p)

## Slide 39
Course Summary
VI. Surfaces:
Surface excess properties;
Surface area and curvature;
Laplace equation (pressure versus curvature/size);
Contact angle;
Kelvin equation (vapor pressure for a droplet/bubble);
Solubility versus size;
Critical nucleus size;
Ostwald ripening;
Heterogeneous versus homogeneous nucleation;
Gibbs-Thompson and Ostwald-Freundlich equations;
Chemical (irreversible) or physical adsorption (reversible);
Adsorption isotherm (Langmuir, BET);
Block copolymers;

## Slide 40
Laplace Equation
For a 100 nm (1e-5 cm) droplet of water in air (72 e-7 J/cm2 or 7.2 Pa-cm)
Pressure is 720 MPa (7,200 Atmospheres)
-S U V
H A
-p G T
c is curvature 1/r

## Slide 41
Dihedral angles

## Slide 42
Young Dupre Equation

## Slide 43
Pressure for equilibrium of a liquid droplet of size ”r”
Reversible equilibrium
At constant temperature
Differential Laplace equation
Small drops evaporate, large drops grow
-S U V
H A
-p G T

## Slide 44
Solubility and Size, r
Consider a particle of size ri in a solution of concentration xi with activity ai
Derivative form of the Laplace equation
Dynamic equilibrium
For an incompressible solid phase
Definition of activity
Solubility increases exponentially with reduction in size, r
(xil)r = (xil)r=∞ exp(2gsl/(rRT r))
Small particles dissolve to build large particles with lower solubility
-To obtain nanoparticles you need to supersaturate to a high concentration (far from equilibrium).
-Low surface energy favors nanoparticles. (Such as at high temperatures)
-High temperature and high solid density favor nanoparticles.
Supersaturation is required for any nucleation

## Slide 45
Critical Nucleus and Activation Energy for Crystalline Nucleation (Gibbs)
(M/r)is molar volume
Surface increases free energy
Bulk decreases free energy
Barrier energy for nucleation at the critical nucleus size beyond which growth is spontaneous

## Slide 46
Critical Nucleus and Activation Energy for Crystalline Nucleation (Gibbs)
DfusGm = DfusHm - TDfusSm
Lower T leads to larger DfusGm (Driving force for crystallization)
smaller r* and smaller Dl-sG*
Deep quench, far from equilibrium leads to nanoparticles

## Slide 47
Ostwald Ripening
Dissolution/precipitation mechanism for grain growth
Consider small and large grains in contact with a solution
Grain Growth and Elimination of Pores

## Slide 48
Formation of a surface nucleus versus a bulk nucleus from n monomers
Homogeneous
Heterogeneous (Surface Patch)
Surface energy from the sides of the patch
Bulk vs n-mer
So surface excess chemical potential

## Slide 49
Barrier is half the height for nucleation
Size is half

## Slide 50
Three forms of the Gibbs-Thompson Equation
Ostwald-Freundlich Equation
x = supersaturated mole fraction
x∞ = equilibrium mole fraction
n1 = the molar volume
Free energy of formation for an n-mer nanoparticle from a supersaturated solution at T
Difference in chemical potential between a monomer in supersaturated conditions and equilibrium with the particle of size r
At equilibrium
For a sphere

## Slide 51
Three forms of the Gibbs-Thompson Equation
Ostwald-Freundlich Equation
Areas of sharp curvature nucleate and grow to fill in. Curvature k = 1/r
Second Form of GT Equation

## Slide 52
Three forms of the Gibbs-Thompson Equation
Third form of GT Equation/ Hoffman-Lauritzen Equation
B is a geometric factor from 2 to 6
Crystallize from a melt, so supersaturate by a deep quench
Free energy of a crystal formed at supercooled temperature T

## Slide 53
Adsorption Isotherms
Bg-Gas species (N2)
Bmon – Adsorbed (N2) in an occupied surface site
Vmon – Available surface site
aBg is activity of B in the gas phase
q = GB/GBMax Fractional Coverage
Langmuir Adsorption Isotherm
GBMax Is the coverage for a monolayer.
Equilibrium Constant:

## Slide 54
Derivation of Langmuir Equation (as derived by Hill)
Langmuir Equation is for equilibrium of a monolayer with a solution of concentration x2
A surface has adsorption sites that can hole solvent (1) or solute (2)
Some fraction of the surface bound to solute, x2b, and some fraction to solvent, x1b.
The concentration of solute in the solution ((partial pressure or pressure)/saturated pressure) is x2s = q
The equilibrium involves x1b + x2s  x1s + x2b
The equilibrium constant is given by, K = (x1b x2s)/(x1s x2b) = (1 - x2b) q /((1 - q) x2b)
Rearranging yields q = Kx2b/(1 - x2b + K x2b) ~ Kx2b/(1 + K x2b) = p/p0

## Slide 55
Derivation of BET Theory
Langmuir Equation is for monolayers
BET is for multilayers where the first layer has an energy of adsorption, E1, and second and higher layers use the energy of liquification, EL
Langmuir Equation is applied for each layer (gas and adsorbed layer are at dynamic equilibrium)
At Psat the surface is in the liquid (For Langmuir this was a monolayer)
Fractional coverage of layer i, qi
Rate of adsorption on layer i-1 to fill layer i, Ri-1,ads = ki,ad P qi-1
Rate if desorption from layer I, Ri,des = ki,des qi
ki,ads = ki,des = exp(-Ei/kT)
nm = monolayer amount of gas
n = experimental amount of gas adsorbed

## Slide 56
How can you predict the phase size? (Meier and Helfand Theory)
Consider lamellar micro-phase separation.
dA
dB
dt
Perfect match

## Slide 57
Course Summary
VII. Heat of Formation:
Dependencies in periodic table;
Electronegativity;
Energetics of formation (electrostatic, repulsion, dispersion, polarization, crystal field);
Atomic size (perovskites, spinels, zeolites);
Substitutional solids;
Conformational entropy of polymers

## Slide 58
Electronegativity, the ability of an atom to attract electrons in a bond
Linus Pauling

## Slide 59
p-orbitals
6 valence electrons
(more acidic to right)
s-orbitals
2 valence electrons
(more basic to right)
Acidic
Basic
d-orbitals
10 valence electrons
Transition
Metals
f-orbitals
14 valence electrons
Basic (at low oxidation state)
Acidic (at high oxidation state)

## Slide 60
Energetics of compound formation
Electrostatic attraction +-
Electron electron repulsion
Van der Waals or dispersion (d+ makes d- leads to net attraction)
Polarization (shifting within compound of electrons)
Crystal field effects

## Slide 61
Conformational Enthalpy of Polymers
The Rotational Isomeric State Model of Volkenstein and Paul Flory (Nobel Prize)
Carbon has a tetrahedral bonding arrangement
For a chain of carbon the two side groups interact with the side groups of neighboring carbons
“Trans” is sterically the most favorable arrangement
“Gauche +” and “Gauche -” are less favorable
The Boltzmann equation gives the probability of a particular conformation, Z is the partition function or the sum of all of the different Boltzmann expressions in an ensemble
For Butene

## Slide 62
Conformational Enthalpy of Polymers
The Rotational Isomeric State Model of Volkenstein and Paul Flory (Nobel Prize)
For a polymer with N carbons there are N-2 covalent bonds
The number of discrete conformation states per chain is nN-2 where n is the number of discrete rotational states for the chain, tttt, g-g-g-g-,g+g+g+g+,g+ttt, etc. for N = 4; N1=1, N4=4, etc. assuming no end effects
Average rotational angle
Characteristic Ratio
Q is the bond angle
180°-109° = 71°
Eg+- = 2100 J/mole
C∞ = 3.6
Exp. 6.7

## Slide 63
Course Summary
VIII. Heat Capacity:
Cp-Cv;
Internal energy of a gas;
Dulong-Petit Law for solids;
Phonons; longitudinal; transverse; optical; acoustic
Brillouin Zones;
Acoustic phonons; Optical Phonons
Density of states;
Bose-Einstein statistics;
Einstein model;
Debye model;
Dispersion relations;
Debye temperature; Debye frequency;
Modulus and heat capacity;
Grüneisen parameter Cp-Cv
Spectroscopy; density of states; heat capacity;
Entropy from heat capacity;
Heat capacity from group contribution;
Electronic heat capacity;
Heat capacity at second order transitions;
Heat capacity of polymers

## Slide 64
Heat Capacity
DSC
Heat is not a state function, so we define a state function related to heat, dS = dQ/T
-S U(E) V
H A(F)
-p G T
dH = VdP + TdS
At constant P (dH = TdS = dQ)P
We have Cp = (dH/dT) P = (dQ/dT) P
In the DSC we measure the heat flow dQ/dt (Watts) at a constant heating rate dT/dt at constant pressure,
(dQ/dT) P = Cp
So, the y-axis is Cp times dT/dt the latter of which is constant

## Slide 65
Cp = (dH/dT) P = (dQ/dT) P = ((dQ/dt) / (dT/dt))P

## Slide 66
Derive the expression for Cp – CV
Cp - Cv = a2VT/kT
a = (1/V) (dV/dT)p
kT = (1/V) (dV/dP)T
CV = (dU/dT)V
From the Thermodynamic Square
dU = TdS – pdV so CV = (dU/dT)V = T (dS/dT)V - p (dV/dT)V
Second term is 0 dV at constant V is 0
(dS/dT)V = CV /T
Similarly
Cp = (dH/dT)p
From the Thermodynamic Square
dH = TdS + Vdp so Cp = (dH/dT)p = T (dS/dT)p - V (dp/dT)p
Second term is 0 dp at constant p is 0
(dS/dT)p = Cp /T
Write a differential expression for dS as a function of T and V
dS = (dS/dT)VdT + (dS/dV)TdV using expression for CV above and Maxwell for (dS/dV)T
dS = CV /T dT + (dp/dT)VdV use chain rule: (dp/dT)V = -(dV/dT)p (dP/dV)T = Va / (VkT)
Take the derivative for Cp: Cp/T = (dS/dT)p = CV /T (dT/dT)p + (a/kT)(dV/dT)p = CV /T + (Va2/kT)
Cp - Cv = a2VT/kT
-S U V
H A
-p G T
From Chapter 1

## Slide 68
Monoatomic H(g) with only translational degrees of freedom is already fully excited at low temperatures. The vibrational frequencies (n) of H2(g) and H2O(g) are much higher, in the range of 100 THz, and the associated energy levels are significantly excited only at temperatures above 1000 K. At room temperature only a few molecules will have enough energy to excite the vibrational modes, and the heat capacity is much lower than the classical value. The rotational frequencies are of the order 100 times smaller, so they are fully excited above ~10 K.

## Slide 69
Atoms in a crystal (Dulong and Petit Model)
Works at high temperature
Three Harmonic oscillators, x, y, z
Spring (Potential Energy)
dU/dx = F = -kx where x is 0 at the rest position
U = -1/2 kx2
Kinetic Energy
U = ½ mc2
Three oscillator per atom so Um = 3RT
dU = -pdV + TdS
d(U/dT) V = T(dS/dT) V = CV
-SUV
H A
-pGT
Each atom in a solid has 6 springs
Each spring with ½ kT energy
So, 6/2R = 3R = Cv

## Slide 70
Phonons
Two size scales, a and l
If l ≥ a you are within a Brillouin Zone
Wavevector k = 2p/l
A phonon with wavenumber k is thus equivalent to an infinite family of phonons with wavenumbers k ± 2π/a, k ± 4π/a, and so forth.
k-vector is like the inverse-space vectors for the lattice
It is seen to repeat in inverse space making an inverse lattice
Brillouin zones, (a) in a square lattice, and (b) in a hexagonal lattice
those whose bands become zero at the center of the Brillouin zone are called acoustic phonons, since they correspond to classical sound in the limit of long wavelengths. The others are optical phonons, since they can be excited by electromagnetic radiation.

## Slide 71
Phonons
Two size scales, a and l
If l ≥ a you are within a Brillouin Zone
Wavevector k = 2p/l
The density of states is defined by
The partition function can be defined in terms of E or in terms of k
E and k are related by the dispersion relationship which differs for different systems
For a longitudinal Phonon in a string of atoms the dispersion relation is:

## Slide 72
Phonons
Bose-Einstein statistics gives the probability of finding a phonon in a given state:

## Slide 73
Phonons
Dispersion relation for phonons
Plus optical
Minus Acoustic

## Slide 74
Einstein Model
Works at low and high temperature
Lower at low temperature
Quantized energy levels
Bose-Einstein statistics determines the distribution of energies
The mean “n” at T is given by
Average energy for a crystal with three identical oscillators

## Slide 75
Einstein Model
Works at low and high temperature
Lower at low temperature
Average energy for a crystal with three identical oscillators
Einstein temperature:

## Slide 76
Dispersion Curve
Angular frequency of vibrations as a function of wavevector, q
First Brillouin Zone of the one-dimensional lattice
Longer wavevectors are smaller than the lattice

## Slide 77
Longitudinal and Transverse dispersion relationships for [100],[110], and [111] for lead
Transverse degenerate for [100] and [111] (4 and 3 fold rotation axis)
Not for [110] (two fold rotation axis)

## Slide 78
Higher Characteristic T represents stronger bonds

## Slide 79
Higher Characteristic T represents stronger bonds

## Slide 80
Modulus and Heat Capacity
= E e
F/A = E Dd/d
F = K Dd
K = F/Dd = E A/d
At large q, w = √(4K/m)
This yields wD from E
For Cu, qD = 344K
wD = 32 THz
K = 13.4 N/m
wD = 18 THz

## Slide 81
Spectroscopy measures vibrations, this can be used to calculate the density of states, this can be integrated to obtain the heat capacity
Number of vibrational modes
IR: High Polarity Motion of charged atoms under electromagnetic field
NaCl
Raman: High Polarizability
Motion of electrons in polarizable bonds under electromagnetic field
Benzene, Graphene, Nanotubes,

## Slide 82
CV = (dU/dT)V
From the Thermodynamic Square
dU = TdS – pdV so CV = (dU/dT)V = T (dS/dT)V - p (dV/dT)V
Second term is 0 dV at constant V is 0
(dS/dT)V = CV /T
Similarly
Cp = (dH/dT)p
From the Thermodynamic Square
dH = TdS + Vdp so Cp = (dH/dT)p = T (dS/dT)p - V (dp/dT)p
Second term is 0 dp at constant p is 0
(dS/dT)p = Cp /T
Integrate Cp/T dT or Integrate CV/T dT to obtain S
-SUV
H A
-pGT
Entropy from Heat Capacity
Low Temperatures Solve Numerically
High Temperatures Series Expansion

## Slide 83
A striking example is the electronic heat capacity coefficients observed for Rh–Pd–Ag alloys given in Figure 8.22 [17]. In the rigid band approach the addition of Ag to Pd gives an extra electron per atom of silver and these electrons fill the band to a higher energy level. Correspondingly, alloying with Rh gives an electron hole per Rh atom and the Fermi level is moved to a lower energy. The variation of the electronic heat capacity coefficient with composition of the alloy maps approximately the shape of such an electron band.
Add an electron from Ag raises Fermi level
Add a hole from Rh reduces n(eF)

## Slide 84
From Kittel and Kroemer Thermal Physics Chapter 2
For a system with quantized energy and two states e1 and e2, the ratio of the probabilities of the two states is given by the Boltzmann potentials, (t is the temperature kBT)
If state e2 is the ground state, e2 = 0, and the sum of exponentials is called the partition function Z, and the sum of probabilities equals 1 then,
Z = exp(-e2/t) + 1
Z normalizes the probability for a state “s”
P(es) = exp(-es/t)/Z
The average energy for the system is

## Slide 85
Heat Capacity of Polymers
Amorphous structure but with regular order along the chain
1-d vibrational structure
Natoms = number of atoms in a mer unit
3 for CH2
N = number of skeletal modes of vibration
N = 2 for -(CH2)n-
Einstein method works well above 100K

## Slide 86
Course Summary
IX. Solution Models and Equations of State:
Regular solution;
Quasi-regular solution with lattice vibrations;
Accounting for correlations (mean field or specific interactions);
Virial approach for mean field;
Correlation function for specific interactions;
Van der Waals model;
Margulis model; Margulis acid-base;
Redlich-Kister model (asymmetric phase diagrams);
Scatchard-Hildebrand theory (volume versus mole fraction);
Flory-Huggins model (polymers based on volume fraction);
Group Contribution Models:
Hydrogen bonding MOSCED (Modified separation of cohesive energy density); SSCED (Simplified separation of cohesive energy density);
Local Clustering Models: Wilson’s equation; NRTL (Non-random two liquid model);
Surface area rather than volume fraction for interactions: UNIQUAC (Universal quasi-chemical model);
UNIFAC (Universal functional activity coefficient model);
Solutions with multiple sublattices (NaCl);
Order-disorder systems
Order parameter
Non-stoichiometric compounds (perovskite oxides)

## Slide 87
Regular Solution Solution Model
µA ~ dG/dxA

## Slide 88
Excess molar Gibbs energy of mixing for quasi-regular solution
G = H –TS so first term is enthalpic, second is entropic
t is a characteristic temperature, when T = t ideal solution behavior is seen

## Slide 89
Correlations
Dilute: Ideal behavior, there are no interactions
Semi-dilute: weak or strong interactions are possible
With weak interactions the system can be treated with a “mean field”. No correlation is observed, we can use the second virial coefficient and Hildebrand Model
With strong interactions we need to use detailed information about interactions, correlation function or other models

## Slide 91
Margulis one-parameter Model
Chapter 11 Elliot and Lira
Hildebrand Model
Margulis acid-base Model

## Slide 92
Course Summary
X. Thermodynamics and Materials Modeling:
Quantum mechanics (ab initio method, electronic wave functions, nuclei don’t move);
Density functional theory (Minimize E(r) as a function of r(r));
Molecular dynamics modeling (potential fields between atoms);
Mesoscale models (coarse graining; short range interaction potentials);
Dissipative particle dynamics (DPD);
Monte Carlo Metropolis method;
Ising model;
Packages to do materials simulations of different types: LAMMPS; HOOMD-blue; ESPResSo; etc.
Free servers for simulations from Google: Colaboratory

## Slide 93
Coarse Grain Simulations
DPD Simulations
Machine Learning
Data Mining Techniques
Thermodynamics and Materials Modeling

## Slide 94
Quantum mechanical/ab initio methods
Electronic wavefunction is independent of the nuclei since electrons are much smaller and move much faster: Born Oppenheimer Approximation
Solve the Schrodinger equation
Hamiltonian in atomic units:
ri electron positions; da nuclear positions, Za nuclear charge
Kinetic Energy – e- nuc. attraction + e- e- repulsion + Nuc. Nuc. repulsion
Solve approximately since true wave function can’t be found directly. Compare proposed function results with data. Variational Principle: lowest energy wins.
4) Obey Pauli exclusion principle.

## Slide 95
Density functional theory
Ground state can be obtained through minimization of E(r) of r(r)
Parallel non-interacting system (NIS)
3) Write the energy functional as
KE of NIS + e- nuc. int. + Coulomb + exchange correlation energy
Minimize E[r] to obtain wave functions then iterate to obtain the ground
state density and energy

## Slide 96
Molecular Dynamics
Generate initial condition with particles identified by position and velocity
Calculate the force on each particle using potentials
Forces (accelerations) remain constant for a time step, position and velocity change
Repeat 3) until temperature is constant
After steady state record velocities and positions so that <r2> = 6Dt is found
Time calculation is on the order of nanoseconds.
Neither Monte Carlo nor Molecular Dynamics can calculate the free energy since they ignore large energy regions of phase space
They can calculate differences in free energy for phase diagram construction

## Slide 97
Coarse Grain Simulations
DPD Simulations
Machine Learning
Data Mining Techniques

## Slide 98
Coarse Grain Simulations
DPD Simulations
Machine Learning
Data Mining Techniques

## Slide 99
Monte Carlo/Metropolis Method
Periodic Boundary Conditions
Fix T, V, N
“Z” is a state of the system
Calculate f(Z) by molecular mechanics with potentials
Accept a configuration “Z” if it has a low energy relative to kT with some randomness
Calculate the average
Start with a random configuration calculate f(Z)
Move one atom or molecule or group of molecules
Calculate f(Z’) if lower than f(Z) accept
If higher than f(Z) calculate exp(-Df/kT) and a random number from 0 to 1
If higher than random number accept
Repeat

## Slide 100
Dissipative Particle Dynamics (DPD)

## Slide 101
Course Summary
XI. Experimental Thermodynamics
Calorimetry
Differential Scanning Calorimetry
Modulated DSC
Microcalorimetry
Differential Thermal Analysis
Thermal Gravimetric Analysis
Bomb Calorimetry/Combustion Calorimetry
And 25 other techniques

## Slide 102
Course Summary
I. Introduction
II. Single component systems
III. Solutions
IV. Phase diagrams
V. Phase stability
VI. Surfaces
VII. Heat of formation
VIII. Heat capacity
IX. Solution models and equations of state
X. Thermodynamics and materials modeling
XI. Experimental methods