## Slide 1
Experimental Thermodynamics (30 common techniques)
Thermal analysis
Calorimetry
Differential Scanning Calorimetry
Modulated DSC
Microcalorimetry
Differential Thermal Analysis
Bomb Calorimetry/Combustion Calorimetry
Thermal Gravimetric Analysis/DTA/MS/IR/Raman
Colligative Analysis
Membrane Osmometry
Vapor Pressure Osmometry
Melting point/Boiling point
Density
Archimedes Method
Helium Pycnometry
Density Gradient Column
Dilatometry
Sound Velocity
Shock Compression
Abbe Refractometer
Ellipsometer
Surfaces
Gas Adsorption
Contact Angle
Zeta Potential
X-ray and Neutron Reflectivity
Phase Structure
Light, X-ray, Neutron Scattering
Osmotic Compressibility
OM, SEM, TEM, AFM
XRD, NPD
Chemical Methods

## Slide 2
Calorimetry
Thermal analysis
Calorimetry
Differential Scanning Calorimetry
Modulated DSC
Microcalorimetry
Differential Thermal Analysis
Thermal Gravimetric Analysis
Bomb Calorimetry/Combustion Calorimetry

## Slide 3
Calorimetry
How to build a scanning calorimeter
What is needed?
One or Two Adiabatic/Isolated Cells
Thermocouples, T
Heating rate, dQ/dt
Mass, m
Simplest approach and useful for very low or very high temperatures is differential thermal analysis DTA
DTA is a simple design for difficult environments
Two cells heated at same rate and the difference in temperature is recorded
Differences in heat capacity and latent heats create differences in temperatures through transitions.
dT/dQ is measured in the DTA
dQ/dT is measured in the DSC

## Slide 4
Measure the Temperature
Seebeck Effect: Thermocouple
Electrons (or holes) flow from the hot side where they have high kinetic energy to the cold side where they have less kinetic energy. They will spend more time in the cold side, something like condensing in the cold side. This effect is different in magnitude for different metals or semiconductors. The difference in potential at the cold side between two metals is proportional to the temperature. (Similar to thermophoretic sampling.)
Thermoelectric generator
Thermally insulating
Electrically conducting
Thermocouple

## Slide 6
Calorimetry
Cryostat
Use liquid He or a He refrigerator
4.2K boiling point

## Slide 7
Calorimetry
dQ/dt = Cp dT/dt + DHtransitions
DQ = Cp (Tf-Ti)+ DHtransitions
Tf = Ti + (DQ – DHtransitions)/Cp
DQ = (dQ/dt) t
dT/dQ is measured in the DTA
dQ/dt = (dT/dt)/(dT/dQ)
dQ/dT is measured in the DSC
dQ/dt = (dQ/dT) (dT/dt)

## Slide 8
Modulated DSC

## Slide 22
Micro Calorimetry (isothermal shown)

## Slide 25
Thermogravimetric Analysis (TGA)

## Slide 26
Thermogravimetric Analysis (TGA)

## Slide 30
TGA/MS
GC
IR
Raman
Etc.

## Slide 31
Membrane Osmometry
P = rgh
Van der Waals
b = Excluded volume
a = attractive potential
Van der Waals Equation P = P

## Slide 32
Archimedes Method for Density
Helium Pycnometry
Helium density
Boyle’s Law (P1V1 = P2V2)
Measure pressure change to get volume
Weigh sample
“Open pore” density

## Slide 33
Density Gradient Column

## Slide 34
Mercury Dilatometry for Thermal Expansion Coefficient, a

## Slide 35
Abbe Refractometer

## Slide 36
Index (and thickness) of thin films Ellipsometer

## Slide 37
Surfaces:
Gas Adsorption

## Slide 39
X-ray and Neutron Reflectivity

## Slide 47
Small-Angle Light, Neutron, and X-ray Scattering for Osmotic Compressibility
Small size
(2p/1) Å = 0.6 nm
Large size
(2p/0.001) Å = 600 nm
“Thermodynamic Limit”
At large sizes contrast arises from thermally driven fluctuations in density that are opposed by the osmotic compressibility, (dr/dP)T The observed intensity I(q=>0) ~ kT/ (dr/dP)T
Here P is P the osmotic pressure which can be expressed using the virial expansion so that the first derivative is the second virial coefficient A2. Low-q scattering can measure the thermodynamic interaction of particles.

## Slide 48
Low-q scattering allows measurement of the second virial coefficient B2
Notes: Kinetic distribution and dispersion of nanoparticles in polymer nanocomposites.
Fri. March 10, 11:54 a.m. – 12:06 p.m. PST
Room 128
Dispersion and distribution of nanoparticles in polymer mixing processes are stumbling blocks to the production of nanocomposites. Dispersion, in polymer processing, refers to the structural breakup of agglomerates of nanoparticles while distribution involves spatial randomization. These two features of mixing respond to different viscous flow regimes: laminar flow and turbulent flow. Distributive mixing is difficult in laminar flow, while dispersive structural change can result from either laminar or turbulent flow. In kinetic mixing, agglomerates of immiscible nanoparticles or aggregates on the nanoscale are dispersively broken apart in proportion to the accumulated strain. Parallel to this structural change, turbulent flow, related to the Reynolds number, convectively redistributes the nanoparticles or aggregates. This redistribution optimally leads to the formation of macroscopic filler networks completing a structural hierarchy necessary for ionic and electrical conductivity, tear strength, and modulus enhancement. Both distribution and dispersion depend on the velocity of flow, but they have inverse dependencies on the flow gap size in the simplest geometry. We have adapted the random phase approximation and the van der Waals model to understand kinetic dispersion and distribution in polymer nanocomposites.

## Slide 49
Experimental Thermodynamics (30 common techniques)

## Slide 50
Experimental Thermodynamics (30 common techniques)

## Slide 51
Experimental Thermodynamics (30 common techniques)

## Slide 52
Experimental Thermodynamics (30 common techniques)

## Slide 53
Experimental Thermodynamics (30 common techniques)

## Slide 54
Experimental Thermodynamics (30 common techniques)

## Slide 55
Experimental Thermodynamics (30 common techniques)

## Slide 56
Experimental Thermodynamics (30 common techniques)

## Slide 57
Experimental Thermodynamics (30 common techniques)

## Slide 58
Experimental Thermodynamics (30 common techniques)

## Slide 59
Experimental Thermodynamics (30 common techniques)

## Slide 60
Experimental Thermodynamics (30 common techniques)