## Slide 1
Heat Capacity
DSC
Heat is not a state function, so we define a state function related to heat, dS = dQ/T
-S U(E) V
H A(F)
-p G T
dH = VdP + TdS
At constant P (dH = TdS = dQ)P
We have Cp = (dQ/dT) P = (dH/dT) P
In the DSC we measure the heat flow dQ/dt (Watts) at a constant heating rate dT/dt at constant pressure,
(dQ/dT) P = Cp
So, the y-axis is Cp times dT/dt the latter of which is constant
dS = dQ/T

## Slide 2
Cp = (dH/dT) P = (dQ/dT) P = ((dQ/dt) (dT/dt))P

## Slide 3
Derive the expression for Cp – CV
Cp - Cv = a2VT/kT
a = (1/V) (dV/dT)p
kT = (1/V) (dV/dP)T
CV = (dU/dT)V
From the Thermodynamic Square
dU = TdS – pdV and, CV = (dQ/dT) V = T (dS/dT)V - p (dV/dT)V = (dU/dT)V
Second term is 0, dV at constant V is 0
(dS/dT)V = CV /T
Similarly
Cp = (dH/dT)p
From the Thermodynamic Square
dH = TdS + Vdp so Cp = (dH/dT)p = T (dS/dT)p - V (dp/dT)p
Second term is 0, dp at constant p is 0
(dS/dT)p = Cp /T
Write a differential expression for dS as a function of T and V
dS = (dS/dT)VdT + (dS/dV)TdV using expression for CV above and Maxwell for (dS/dV)T
dS = CV /T dT + (dp/dT)VdV use chain rule: (dp/dT)V = -(dV/dT)p (dP/dV)T = Va / (VkT)
Take the derivative for Cp: Cp/T = (dS/dT)p = CV /T (dT/dT)p + (a/kT)(dV/dT)p = CV /T + (Va2/kT)
Cp - Cv = a2VT/kT
-S U V
H A
-p G T
From Chapter 1
dS = dQ/T
dU = TdS – PdV
dH = TdS + VdP
dQ = TdS

## Slide 4
Molecular Basis for the Heat Capacity (Gasses)
Internal Energy of a gas
For an ideal gas, the potential is 0
Monoatomic Gas: Ar
3 translational degrees of freedom each with ½ kT energy
Linear molecule, CO2, can rotate in two axes, CV,m = 5/2 R
Non-Linear, H2O, can rotate in three axes, CV,m = 6/2 R
Plus, vibrational degrees of freedom

## Slide 5
We calculate CV since all models assume constant volume
We measure Cp since calorimetric measurements are made at atmospheric pressure
From CV for an ideal gas, you add R to obtain Cp
For an ideal gas PV = RT
a is (dV/dT)p/V = R/PV = 1/T
is -(dV/dP)T/V = RT/P2V = 1/P
Cp – Cv = (1/T)2 (TV) P = PV/T = R
For other materials you need to know the thermal expansion coefficient and compressibility as a function of temperature.

## Slide 6
Heat Capacity, multi-atomic gasses and vibrations
Linear molecule, CO2, can rotate in two axes, CV,m = 5/2 R
Non-Linear, H2O, can rotate in three axes, CV,m = 6/2 R
Plus, vibrational degrees of freedom
Potential and Kinetic degrees of vibrational freedom add 2(R/2) for each type of vibration
Generally, 3n-6 vibrational modes
(For linear 3n-5 so for CO2 4 modes symmetric stretch, asymmetric stretch, two dimensions of bend)

## Slide 7
For an ideal gas
= 1/V (dV/dT) = R/PV = 1/T
= -1/V (dV/dP) = RT/VP2 = 1/P
a2TV/kT = VP/T = R
PV = RT
dV/dT = R/P
dV/dP = -RT/P2

## Slide 9
Monoatomic H(g) with only translational degrees of freedom is already fully excited at low temperatures. The vibrational frequencies (n) of H2(g) and H2O(g) are much higher, in the range of 100 THz, and the associated energy levels are significantly excited only at temperatures above 1000 K. At room temperature only a few molecules will have enough energy to excite the vibrational modes, and the heat capacity is much lower than the classical value. The rotational frequencies are of the order 100 times smaller, so they are fully excited above ~10 K.
3R = 25 J/(mol K)
J/(mol K)
20.8
37.5
58.3
Ideal Gasses

## Slide 10
Monoatomic H(g) with only translational degrees of freedom is already fully excited at low temperatures. The vibrational frequencies (n) of H2(g) and H2O(g) are much higher, in the range of 100 THz, and the associated energy levels are significantly excited only at temperatures above 1000 K. At room temperature only a few molecules will have enough energy to excite the vibrational modes, and the heat capacity is much lower than the classical value. The rotational frequencies are of the order 100 times smaller, so they are fully excited above ~10 K.
Ideal Gasses

## Slide 11
Dulong and Petit Law (Observation, heat capacity of solids)
In the classical statistical theory of Ludwig Boltzmann, the heat capacity of solids approaches a maximum of 3R per mole of atoms because:
full vibrational-mode degrees of freedom amount to 3 degrees of freedom per atom (x, y, z),
each corresponding to a kinetic energy term and a potential energy term.
By the equipartition theorem, the average of each term is 1⁄2kBT per atom, or 1⁄2RT per mole.
Multiplied by 3 degrees of freedom (x, y, z) and the two terms per degree of freedom (kinetic and potential), this amounts to 3R per mole heat capacity.
CV/n = 3R (25 J/(mol K)
Heat Capacity of Solids

## Slide 12
Dulong and Petit Law (Observation for Solids)
Cv

## Slide 13
Dulong and Petit Law (Observation for solids)
Cv
Fails for strongly bound light atoms

## Slide 14
Atoms in a crystal (Dulong and Petit Law)
Works at high temperature
Three degree of freedom oscillators per atom so Um = 3RT
dU = -pdV + TdS
(dU/dT) V = T(dS/dT) V = CV
-SUV
H A
-pGT
Boltzman 1877 Explains
Each atom in a solid has 6 springs
Each spring with ½ kT energy
So, 6/2R = 3R = Cv
Three Harmonic oscillators, x, y, z
Spring (Potential Energy)
dU/dx = F = -Kx where x is 0 at the rest position
U = -1/2 Kx2
Kinetic Energy
U = ½ mc2
c is the velocity of the atom so dx/dt
Force Balance
-K x = m d2x/dt2
Plug in a sine wave solution,
x = A sin(wt)
Yields w = √(K/m)
So, there is a fixed frequency for a fixed spring constant and mass, since E = hw/2p, there is a fixed or quantized energy
Potential and Kinetic Energies balance in an oscillatory spring so U = 0

## Slide 15
Atoms in a crystal (Dulong and Petit Law)
Works at high temperature
Force Balance
-K x = m d2x/dt2
Plug in a sine wave solution,
x = A sin(wt)
Yields w = √(K/m)
So, there is a fixed frequency for a fixed spring constant and mass, since E = hw/2p, there is a fixed or quantized energy
For something like a guitar string, we have quantized energy and frequency, it has one tone, but also overtones so, E = nE1 where n is the mode of vibration or quantized state, and n has integer values starting with 1. E1 is the energy of the primary mode, E = nhn or nhw/2p for the vibration.
For quantum mechanics (very small particles like atoms) there is a problem with E = nhn or nhw/2p
1) At absolute 0 there is a ”zero-point energy” that keeps everything from collapsing for instance, we don’t observe collapse as we approach absolute 0. Schrodinger equation finds this zero-point energy is ½ hn
2) If energy were 0 at absolute 0 then we would know both the position of an atom and its momentum = 0
This would disagree with the Heisenberg uncertainty principle. So, you need a “zero-point energy”
3) A “zero-point energy” can be measured experimentally
E = hn (1/2 + n) and n has integer values starting at 0 for the ground state energy.
Einstein Model

## Slide 16
Einstein Derivation of Dulong Petit
-S U(E) V
H A(F)
-p G T
U = A + TS
dA = -SdT – pdV
(dA/dT)V = -S
U = A - T (dA/dT)V
A = NE0 + NkT
(dA/dT)V = Nk
U = NE0 + NkT
- NkT
= NE0 + gNkT
dlnx = dx/x
g is number of DOF or 3

## Slide 17
Consider the crystal is made up of free atoms confined into boxes as harmonic oscillators in 3D, x, y, z. All the atoms have the same Einstein frequency, nE. There are then, 3N ”independent” harmonic oscillators, where N is the number of moles of atoms in the crystal. First consider one harmonic oscillator using k then multiply by 3N to get 3R.
The energy of one harmonic oscillator for quantum state (mode) “n” is en = hnE (1/2 + n) where n is 0, 1, 2, 3,…,∞
The harmonic oscillators are at equilibrium at temperature T so the partition function (Zustandssumme, sum of states),
= and
Sum of geometric progress series
Note that this explicitly includes the ground state energy, if you start with just an energy you get Z = 1/(1-e-x)
Equipartition theorem: Energy is partitioned according to the probability of states
The average energy = <U> ==
For 3N,
Einstein Model
because

## Slide 18
Phonons
From Dove
Einstein Model
Almost perfect fit, very high value for CV
(see homework paper Caplin Grüner Dunlap)

## Slide 19
Einstein Model
Works at low and high temperature (3R)
Error in dependence near 0K

## Slide 20
Single vibrational mode for all three DOF
Low T behavior exp(QE/T) doesn’t work
Cv follows T3
The deviation is because Einstein ignored that
lattice vibrations are coupled to each other,
not independent
“Collective Lattice Vibrations”
Einstein Model
Works at low and high temperature (3R)
Error in dependence near 0K

## Slide 21
Debye Model
Works

## Slide 22
Electronic Contribution to Heat Capacity (Briefly)
http://vallance.chem.ox.ac.uk/pdfs/EinsteinDebye.pdf
For T < 10K
Einstein Temp.
Copper 236K
Aluminum 294K
Lead 72.8 K
Iron 355K
Grüner Constant

## Slide 23
Phonons
k-vectors exceeding the first Brillouin zone (red) do not carry any more information than their counterparts (black) in the first Brillouin zone.
Two size scales, a and l
If l ≥ a you are within a Brillouin Zone
Wavevector k = 2p/l
Crystal of lattice spacing a; Sound waves of wavelength l or k vector 2p/l
Black are atoms subject to a high frequency transverse (wave) vibration (red)

## Slide 24
Phonons
Two size scales, a and l
If l ≥ a you are within a Brillouin Zone
Wavevector k = 2p/l
A phonon with wavenumber k is thus equivalent to an infinite family of phonons with wavenumbers k ± 2π/a, k ± 4π/a, and so forth.
k-vector is like the inverse-space vectors for the lattice (or the Miller indices)
It is seen to repeat in inverse space making an inverse lattice
Brillouin zones, (a) in a square lattice, and (b) in a hexagonal lattice
those whose bands become zero at the center of the Brillouin zone are called acoustic phonons, since they correspond to classical sound in the limit of long wavelengths. The others are optical phonons, since they can be excited by electromagnetic radiation.

## Slide 25
Phonons
The density of states is defined by
The partition function (Z) can be defined in terms of energy (E), ,
or in terms of the wavevector k=2p/l = 2pE/hc = -2p/hc
E and k are related by the dispersion relationship (dispersion of energy in k) which differs for different systems
(longitudinal, transverse, acoustic, optical phonons)
For a Longitudinal Phonon in a string of atoms the dispersion relation is:
Transverse is like an ocean wave or a guitar string, longitudinal is a compressive wave like sound
Two size scales, a and l
If l ≥ a you are within a Brillouin Zone
Wavevector k = 2p/l
This relates modulus to frequency
sin x = x – x3/3! + x5/5! - …
For small x; sin x = x

## Slide 26
Phonons
Dispersion Relationship is value of energy or frequency of vibrations at a size-scale or wavelengths or what happens to vibrational energy in the crystal, i.e., modulus.
Density of States is how the total energy is distributed to different frequencies of vibration. This is related to what happens at different wavenumbers to different wavelength phonons.
N is an integer related to the vibrational state k

## Slide 27
Frequency of a Harmonic Oscillator
Do a Force Balance
F = mx” = Kx where K is the spring constant, m is the mass
Then mx” – Kx = 0 is a second order differential equation or
x” – (K/m)x = 0
If you know that the derivative of exponential is the exponential
Then you can guess one answer (this helps)
x = exp(±√(K/m) t); x’= ±√(K/m) exp(±√(K/m) t); x” = K/m exp(±√(K/m) t)
√(K/m) and t have to have inverse units so √(K/m) = w
This is the native frequency of the oscillator

## Slide 28
Phonons
Bose-Einstein statistics gives the probability of finding a phonon in a given state:
m is the ground state energy and e is the energy of a state
As temperature increases the number at frequency n increases
As n increases the number at fixed T drops
If n = exp((m-e)/kT)/Z and A/(1-A) = 1/((1/A)-1) and 1/e(x) = e(-x)

## Slide 29
Phonons
Dispersion relation (relating E to k) for phonons (much math to get this expression)
Plus optical
Minus Acoustic
Atoms or ions of mass m1, m2
Separated by a distance a
With spring constant K
2 modes of vibration result for a crystal with two atoms in a primitive cell
+ is optical (atoms move against each other, picture Na+ Cl- subject to an oscillating electric field, i.e. IR light) finite value at k = 0 reflects the polarization of the material i.e. the dielectric constant
is acoustic (atoms move with each other) move at speed of sound. 0 energy at k = 0 or infinite l means motion of the whole object
For three or more atoms in a primitive cell there are Three acoustic modes: One longitudinal (sound) and Two transverse (ocean)
Number of optical models is 3N-3
Fluids can’t support shear stress so, they only have longitudinal (sound) acoustic modes

## Slide 30
Phonons
From Dove
Phonons have energy hw/2p
The energy at 0K is not 0 it is ½ hw/2p
This is a consequence of energy quantization (lattice calculations are done at 0K)
(Uncertainty principle)
n is the number of phonons at wavelength w and temperature T
Bose-Einstein Relationship
Average of some parameter ”q”

## Slide 31
Phonons
From Dove
Bose-Einstein Relationship
At high T
3 vibrations for each atom
E = 3RT
Dulong Petit result for the Bose-Einstein Relationship at high T

## Slide 32
Debye Model (Wikipedia) Why the cutoff in g(n) at nD?
For a cube of size L vibrations are limited to certain modes like a string of length L
cs is the speed of sound in the solid
For 3d
pn is the momentum of a phonon
Modes of vibration, n
For N atoms in the box
This is the highest energy vibration
At high temperature all of the vibrations are excited
(Transverse Wave)

## Slide 33
Debye Model (This is “borrowed” by Rouse for polymer dynamics)
Collective modes of vibration
If atom n vibrates and atoms n+1 and n-1 vibrate, the potential energy of n isn’t independent of the motion of the neighboring atoms.
Before we had F = -Ku for uncoupled pairs
For coupled units
Force
Force Balance
u is POSITION (x) and F is FORCE here
F is ma also Kx also
dU = F dx
(Longitudinal Wave)

## Slide 34
Propose a solution:
Atomic spacing is “a”
Phase
angle d
Angular frequency of vibrations as a function of wavevector, q
This is a dispersion relation relating energy to q or wavelength
Use in the equation of motion and solve for frequency
Force
”n” is the atom index

## Slide 35
Debye Dispersion Relation
Angular frequency of vibrations as a function of wavevector, q
This is a dispersion relation relating energy to q or wavelength
Einstein Dispersion Relation
https://ebrary.net/196904/mathematics/einstein_model_specific_heat_solids
Debye Dispersion Relation

## Slide 36
Phonons
The density of states is defined by
The partition function (Z) can be defined in terms of E or in terms of the wavevector k=2p/l= 2pE/hc
E and k are related by the dispersion relationship which differs for different systems
(longitudinal, transverse, acoustic, optical phonons)
For a longitudinal Phonon in a string of atoms the dispersion relation is:
Transverse is like an ocean wave or a guitar string, longitudinal is a compressive wave like sound
Two size scales, a and l
If l ≥ a you are within a Brillouin Zone
Wavevector k = 2p/l

## Slide 37
Debye Dispersion Relation
Angular frequency of vibrations as a function of wavevector, q
This is a dispersion relation relating energy to q or wavelength
Debye Dispersion Relation
For small qa, sin(qa/2) = qa/2
( to qD related to nmax)
https://ebrary.net/196904/mathematics/einstein_model_specific_heat_solids
Einstein Dispersion Relation

## Slide 38
Dispersion Curve
Angular frequency of vibrations as a function of wavevector, q
First Brillouin Zone of the one-dimensional lattice
Longer wavevectors are smaller than the lattice

## Slide 39
Dispersion Curve
Angular frequency of vibrations as a function of wavevector, q
First Brillouin Zone of the one-dimensional lattice
Longer wavevectors are smaller than the lattice
Slope is related to
the modulus

## Slide 40
Phonons
k-vectors exceeding the first Brillouin zone (red) do not carry any more information than their counterparts (black) in the first Brillouin zone.
Two size scales, a and l
If l ≥ a you are within a Brillouin Zone
Wavevector k = 2p/l

## Slide 41
Dispersion Curve
Angular frequency of vibrations as a function of wavevector, q
For small wave vectors (long wavelength) sin(q) => q
Long wavelengths
Acoustic or Ultrasonic range
Acoustic or Ultrasonic Range
Group Velocity = dw/dq = a√(K/m)
Speed of sound in the solid
Material is a continuum at these large distances

## Slide 42
Dispersion Curve
Angular frequency of vibrations as a function of wavevector, q
For large wave vectors (short wavelengths)
Dispersion region
isn’t proportional to q
For larger q velocity drops until it stops at the Brillouin zone boundary
Standing Wave

## Slide 43
Longitudinal versus Transverse Waves
There are 2 transverse waves
If material is isotropic or for symmetric crystal planes they are degenerate
In plane and out of plane

## Slide 44
Longitudinal and Transverse dispersion relationships for [100],[110], and [111] for lead
Transverse degenerate for [100] and [111] (4- and 3-fold rotation axis)
Not for [110] (two-fold rotation axis)

## Slide 45
Diatomic Chain Model
Acoustic and Optical modes
Minus Acoustic
Plus Optical

## Slide 46
Physics of Condensed Matter
By Prasanta Misra

## Slide 47
http://www.chembio.uoguelph.ca/educmat/chm729/Phonons/optical.htm

## Slide 48
Phonons
Dispersion relationship is how the energy or frequency of vibrations related to the size scale or wavelengths or what happens to vibrational energy in the crystal, i.e., modulus.
Density of states is how the total energy is distributed to different frequencies of vibration. This is related to what happens at different wavenumbers to different wavelength phonons.
N is an integer related to the vibrational state k
Short sizes (long wavelengths) are high energy (frequency)
Probability of energy going to different frequencies due to the structure

## Slide 49
Convert dispersion relation to DOS for a 1D wave in the continuum limit
Density of states doesn’t depend on time so use:
Wave equation
https://eng.libretexts.org/Bookshelves/Materials_Science/Supplemental_Modules_(Materials_Science)/Electronic_Properties/Density_of_States
Choose periodic boundary condition
Apply boundary conditions to
Yields
This only occurs if:
Since:
That is qL = n 2p
n are the modes or the number of waves for a given frequency and the maximum number is how many atoms on a line.
This is a kind of dispersion relation relating energy or frequency to wave vector

## Slide 50
Convert Dispersion relation to DOS For a 1D wave in the continuum limit
https://eng.libretexts.org/Bookshelves/Materials_Science/Supplemental_Modules_(Materials_Science)/Electronic_Properties/Density_of_States
dn =
This number is the density of states (DOS) at a frequency w
For modes in positive and negative “q=space”
A constant density of states like the Einstein Model
Using dispersion relation

## Slide 51
Number of vibrational modes
Dispersion Relationship
Density of States

## Slide 52
3-d Crystal
Transverse and longitudinal optical and acoustic modes exist for 3d crystals.
n atoms in unit cell
3NAn vibrational modes
3NA acoustic modes (Unit cell vibrates as an entity)
3NA(n-1) optical modes (deformation of unit cell)
At high T each mode has kBT (2 springs for each Cartesian coordinate in two directions)
So, heat capacity is 3R
Number of vibrational modes
Dispersion Relationship
Density of States

## Slide 53
Debye Model
At low temperature
Low energy, low frequency vibrations
are excited
These are acoustic mode vibrations
Unit cell vibrates as an entity
Long distances compared to a unit cell

## Slide 54
Debye Model
Derivation
https://eng.libretexts.org/Bookshelves/Materials_Science/Supplemental_Modules_(Materials_Science)/Electronic_Properties/Debye_Model_For_Specific_Heat

## Slide 55
Debye Model
https://en.wikipedia.org/wiki/Debye_model
One Longitudinal Two Transverse
Convert to Spherical Coordinates

## Slide 56
Debye Model
https://en.wikipedia.org/wiki/Debye_model
There are 8 cubes worth of particles in the sphere

## Slide 57
Debye Model
https://en.wikipedia.org/wiki/Debye_model

## Slide 58
Debye Model
https://en.wikipedia.org/wiki/Debye_model
At high T (Dulong-Petit)
So far I can’t do this

## Slide 59
Debye Model
https://en.wikipedia.org/wiki/Debye_model

## Slide 60
Debye Model
https://en.wikipedia.org/wiki/Debye_model
x = TD/T

## Slide 61
Debye Model
https://en.wikipedia.org/wiki/Debye_model

## Slide 62
Debye Model
Einstein
Debye
https://en.wikipedia.org/wiki/Debye_model

## Slide 63
Debye Model
Einstein
Debye
https://en.wikipedia.org/wiki/Debye_model
Low T
High T
Dulong Petit
Exponential approach to T = 0

## Slide 64
https://lampx.tugraz.at/~hadley/ss1/phonons/table/dosdebye.html

## Slide 65
https://lampx.tugraz.at/~hadley/ss1/phonons/table/dosdebye.html

## Slide 66
Debye Model
At low temperature
Low energy, low frequency vibrations
are excited
These are acoustic mode vibrations
Unit cell vibrates as an entity
Long distances compared to a unit cell
Distribution of frequencies, g(w), above a cutoff frequency, wD

## Slide 67
Debye Model
At low temperature
Low energy, low frequency vibrations
are excited
These are acoustic mode vibrations
Unit cell vibrates as an entity
Long distances compared to a unit cell
Energy also equals kT
This defines the Debye temperature, qD
Quantized energy levels

## Slide 68
Debye Model
Heat Capacity is given by,
Einstein temperature:
At Low T this reduces to,
The T3 dependence is seen experimentally
Einstein Model

## Slide 69
Higher Characteristic T represents stronger bonds

## Slide 70
Higher Characteristic T represents stronger bonds

## Slide 71
Higher Characteristic T represents stronger bonds

## Slide 72
Higher Characteristic T represents stronger bonds

## Slide 73
Modulus and Heat Capacity
= E e
F/A = E Dd/d
F = K Dd
K = F/Dd = E A/d
At large q, w = √(4K/m)
This yields wD from E
For Cu, qD = 344K
wD = 32 THz
K = 13.4 N/m
wD = 18 THz

## Slide 74
Modulus and Heat Capacity
The Debye Temperature reflects the highest energy, lowest wave vector vibrations so the linear part of the dispersion curve

## Slide 76
How to obtain Cp from calculated CV?
At low T
CV = Cp
The harmonic oscillator model assumes constant volume
So, deviations for constant pressure are related to “anharmonic” vibrations
Anharmonic vibrations contribute to the heat capacity
They also lead to a finite thermal expansion coefficient

## Slide 77
Volume Change part
Volume Change and thermal expansion parts
Anharmonic vs Harmonic Contributions to Heat Capacity
(due to thermal expansion and thermal conductivity)

## Slide 78
Approximate relationships for Cp - CV
If you know the thermal expansion coefficient,
If you don’t know the thermal expansion coefficient
How does the frequency of vibration change with specific volume of a unit cell

## Slide 79
http://lampx.tugraz.at/~hadley/ss1/dbr/dos2cv.html

## Slide 80
Spectroscopy measures vibrations, this can be used to calculate the density of states, this can be integrated to obtain the heat capacity
Number of vibrational modes
IR: High Polarity Motion of charged atoms under electromagnetic field
NaCl
Raman: High Polarizability
Motion of electrons in polarizable bonds under electromagnetic field
Benzene, Graphene, Nanotubes,

## Slide 81
Spectroscopy measures vibrations, this can be used to calculate the density of states, this can be integrated to obtain the heat capacity

## Slide 82
Spectroscopy measures vibrations, this can be used to calculate the density of states, this can be integrated to obtain the heat capacity

## Slide 83
CV = (dU/dT)V
From the Thermodynamic Square
dU = TdS – pdV so CV = (dU/dT)V = T (dS/dT)V - p (dV/dT)V
Second term is 0 dV at constant V is 0
(dS/dT)V = CV /T
Similarly
Cp = (dH/dT)p
From the Thermodynamic Square
dH = TdS + Vdp so Cp = (dH/dT)p = T (dS/dT)p - V (dp/dT)p
Second term is 0 dp at constant p is 0
(dS/dT)p = Cp /T
Integrate Cp/T dT or Integrate CV/T dT to obtain S
-SUV
H A
-pGT
Entropy from Heat Capacity
Low Temperatures Solve Numerically
High Temperatures Series Expansion

## Slide 85
Calorimetrically determine S at high temperature then find the Debye temperature that makes the calculation of S match
Large qD means more stable

## Slide 86
Group Contribution Method for Entropy and Heat Capacity
Sum the component entropy and heat capacities

## Slide 87
or
Entropy correlates with molar volume
Maxwell (dS/dV)T = (dp/dT)V
Triple product (dp/dT)V = -(dV/dT)P (dP/dV)T
Q0 is characteristic T at V0
(dS/dq)T from
-SUV
H A
-pGT

## Slide 88
-SUV
H A
-pGT
dG = -SdT +Vdp
For a transition DG = 0
And
dp/dT = DS/DV
DS and DV have the same sign
This isn’t true with a change in oxidation state or coordination number
entropy
Density = mass/volume
All the Si atoms are tetrahedrally coordinated in pyroxene, while 50% are tetrahedrally coordinated and 50% octahedrally coordinated in garnet. In the ilmenite and perovskite modifications all Si atoms are octahedrally coordinated.
Tetrahedral Si
Octahedral Si
Octahedral Si
50%
50%
Tetrahedral Si
Octahedral Si
Octahedral Si

## Slide 89
Electronic Heat Capacity
Electrons that escape from the valence band to the conduction band have three degrees of freedom so contribute (3/2)R to the heat capacity (Drude Model of conduction)
For monovalent Cu we expect Dulong Petit 3R plus 3/2 R (but we see only 3R so where is the 3/2 R?)
For Cu, (3 + 3/2)R this isn’t seen due to quantization of the electron energy level
Fermi Level = Electron energy level that at equilibrium is 50% occupied
Electrons above this energy are free electrons on average

## Slide 90
n(eF) is the number of electrons at the Fermi level
g is the electronic heat capacity coefficient
N1 is the number of electrons excited by kT
These occupy electronic states in a band of kT about the Fermi level
Heat from 0K to T
Free electron gas at 0 K (shaded)
Excited at T (dashed line)
g is 0 for an insulator and has a value for a metal

## Slide 92
For T < 10K

## Slide 93
A striking example is the electronic heat capacity coefficients observed for Rh–Pd–Ag alloys given in Figure 8.22 [17]. In the rigid band approach, the addition of Ag to Pd gives an extra electron per atom of silver and these electrons fill the band to a higher energy level. Correspondingly, alloying with Rh gives an electron hole per Rh atom and the Fermi level is moved to a lower energy. The variation of the electronic heat capacity coefficient with composition of the alloy maps approximately the shape of such an electron band.
Add an electron from Ag raises Fermi level
Add a hole from Rh reduces n(eF)

## Slide 94
Magnetic Heat Capacity
Magnetic excitation
Magnon
Spin waves
Spin waves are propagating disturbances in the ordering of magnetic materials.
Ferromagnet T3/2 at low T
Slide 93 for density of states

## Slide 96
Cp = (dH/dT) P = (dQ/dT) P = ((dQ/dt) (dT/dt))P
Heat Capacity for Systems that Display a Transition

## Slide 97
Heat Capacity for Systems that Display a Transition
Rate of entropy change with T, Cv = T(dS/dT)V,
-increases as kT approaches the transition temperature.
-At high temperatures all states are active so the change in entropy is small.
This results in a peak in Cv and Cp

## Slide 98
From Kittel and Kroemer Thermal Physics Chapter 2
For a system with quantized energy and two states e1 and e2, the ratio of the probabilities of the two states is given by the Boltzmann potentials, (t is the temperature kBT)
If state e2 is the ground state, e2 = 0, and the sum of exponentials is called the partition function Z, and the sum of probabilities equals 1 then,
Z = exp(-e2/t) + 1
Z normalizes the probability for a state “s”
P(es) = exp(-es/t)/Z
The average energy for the system is

## Slide 99
From Kittel and Kroemer Thermal Physics Chapter 2
Second term increases with ~ exp(-e/kT)
First term decays with (e/kT)2

## Slide 100
Metal-Insulator Transition
First order transition at Ttrs between an insulator g = 0 and a metal g = g met
A quantum transition, critical quantum behavior
Transition can occur on doping of an oxide like Fe2O3
Temperature or Pressure Changes
(dS/dT)p = Cp /T

## Slide 101
Magnetic Order-Disorder Transition
At the Curie temperature material goes from a ferromagnet to a paramagnet and loses magnetic order
This impacts the entropy and heat capacity
Maximum total order-disorder entropy can be calculated, DS
(dS/dT)p = Cp /T

## Slide 102
Co3O4 Transitions
Cathode in Li+ batteries or blue pigment for pottery

## Slide 103
Co3O4 Transitions
The normal spinel contains Co2+ at tetrahedral sites and low-spin Co3+ at octahedral sites. The heat capacity effect observed at T b 900K is in part a low- to high-spin transition of the Co3+ ions and in part a partial transition from normal toward random distribution of Co3+ and Co2+ on the tetrahedral and octahedral sites of the spinel structure. The insert to the figure shows the magnetic order–disorder transition of Co3O4 at around 30 K.
(dS/dT)p = Cp /T

## Slide 105
Two levels with energy spacing e/kB
T > e/kB both levels occupied equally
T< e/kB only lower level occupied
Boltzmann statistics yields
(dS/dT)p = Cp /T

## Slide 106
Schottky Defects
Endothermic formation enthalpy
Entropy associated with disorder of defect location
(dS/dT)V = CV /T
DG =DH - TDS

## Slide 107
Fast Ion Conductors (solid oxide fuel cells high T)
Solid electrolytes for batteries and fuel cells
AgI, I lattice remains intact, Ag+ conductor becomes a liquid
Also, Cu2S, Ag2S. NaS battery
Heat Capacity drops with temperature

## Slide 108
Cp = (dH/dT) P = (dQ/dT) P = ((dQ/dt) (dT/dt))P
Liquids and Glasses

## Slide 109
Liquids and Glasses
Broad minimum in heat capacity
Loss of short-range order with rising T leads to drop in heat capacity
Initially, loss of vibrational degrees of freedom associated with short range order led to decrease in Cp
Later, S increases with T
T(dS/dT)p = Cp

## Slide 110
Liquids and Glasses
Broad minimum in heat capacity
Loss of short-range order with rising T leads to drop in heat capacity
Initially, loss of vibrational degrees of freedom associated with short range order led to decrease in Cp
Later, S increases with T
T(dS/dT)p = Cp
Kauzmann Paradox

## Slide 111
Anomalous behavior of glasses near absolute 0
Debye CV ~ T3 near 0 K
Behavior is due to anharmonic vibrations
(Relaxation phenomena)

## Slide 112
Pseudo-second order transition behavior of glasses
Relaxation phenomena
In glasses

## Slide 113
Pseudo-second order transition behavior of glasses
Relaxation phenomena
In glasses

## Slide 114
Pseudo-second order transition behavior of glasses
Relaxation phenomena
In glasses

## Slide 115
Thermodynamic and Kinetic Fragility
Fragile versus strong glass
Kinetics: Deviation from Arrhenius behavior
= h0 exp(-Ea/kBT)
Scaled Exponential
h = h0 exp(-Ea/kBT)m

## Slide 116
DS = SL-Sglass
m is at Tm

## Slide 120
Heat Capacity of Polymers
Amorphous structure but with regular order along the chain
1-d vibrational structure
Natoms = number of atoms in a mer unit
3 for CH2
N = number of skeletal modes of vibration
N = 2 for -(CH2)n-
Einstein method works well above 100K
E is the heat capacity contribution for each vibration

## Slide 121
Weak Van der Waals interactions between chains described by 3d Debye function
For skeletal modes normal to the chain
Strong covalent interactions along chains described by 1d Debye function
For skeletal vibrations in the chain axis
Linear heat capacity increase from 0 to 200K
Below 50K need more detailed breakup of 1d and 3d vibrations using Debye Approach

## Slide 122
At low frequency 3d vibrations, at high frequency 1d vibrations
1d Tasarov simplification (generates about 1% error versus experimental)

## Slide 123
Polystyrene
Natoms = 16 atoms per unit
NE = 42
θ1 = 285 K
42 total atomic group modes of vibration
Or calculate with the Tasarov Equation
N = 6 skeletal mode vibrations

## Slide 126
Average Energy and the Partition Function
Consider a set of N independent (No Enthalpy) molecules at different energy states, Ni molecules at Ei
The average energy is
The Boltzmann Probability gives and is the partition function
Then
Consider so
For ground state E = 0, Z at T = 0 is 1; for T = ∞, Z is the number of states (degeneracy)
For molecular vibrations E = hw

## Slide 127
1907 Einstein Solid Model for Dulong Petit Law at high kT
Energy is quantized, quantum number is “n” goes from 1 to positive integer values
for the principal quantum number
Smallest quantum of energy is e = hn
Energy for quantum number ”n” is
En = hn(n+1/2) = e(n+1/2)
Total number of quantum states N
Total energy Ne(n+1/2)
Ground state energy m
Geometric Series

## Slide 128
1907 Einstein Solid Model for Dulong Petit Law at high kT
Energy = -kT log (Z); log(1/Z) = -log(Z)
exp(x) = 1 + x+ x2/2! + x3/3! +… At high kT => log(hn/kT)
F is A; E is U

## Slide 129
1907 Einstein Solid Model for Dulong Petit Law at high kT
F is A; E is U
Molar Cv/N = gk or Cv = 3R in 3d

## Slide 131
Phonons
From Dove
Bose-Einstein Relationship
As temperature increases the number at frequency n increases
As n increases the number at T drops

## Slide 132
Phonons
From Dove
Einstein Model for Heat Capacity
E is U

## Slide 133
Phonons
From Dove

## Slide 134
Phonons
From Dove
Phonon Free Energy
Including ground state energy
At high T
F is A Helmholz Free Energy

## Slide 135
Phonons
From Dove
For a crystal sum over all vibrations
F is A Helmholz Free Energy

## Slide 136
From Kittel and Kroemer Thermal Physics Chapter 3
For quantized phonons
This is of the form with x <<1 equals 1/(1-x)
Planck Distribution

## Slide 137
Einstein Model
Works at low and high temperature
Lower at low temperature
Quantized energy levels
Bose-Einstein statistics determines the distribution of energies
The mean “n” at T is given by
Average energy for a crystal with three identical oscillators

## Slide 138
Einstein Model
Works at low and high temperature
Lower at low temperature
Average energy for a crystal with three identical oscillators
Einstein temperature:

## Slide 139
Einstein Model
Works at low and high temperature
Lower at low temperature

## Slide 140
Einstein Model
Works at low and high temperature
Lower at low temperature
Single vibrational mode for all three DOF
Low T behavior exp(QE/T) doesn’t work
Cv follows T3
Lattice vibrations are coupled to each other
Collective Lattice Vibrations

## Slide 141
Debye Model
Works