## Slide 1
Phase Stability
Phase Stability

## Slide 2
DG = DH – T DS
Supercool/Superheat/Supersaturate
At the equilibrium melting/freezing point or equilibrium concentration for precipitation the driving force for phase separation, DG = DH – T DS = 0. So, a phase will only form by lowering the temperature below the melting point or increasing the concentration above the solubility limit. This is related to “critical slowing down”. At the critical point nothing happens, or anything can happen, there is no thermodynamic direction for the process.
Cooling below the melting point produces a supercooled liquid, raising the concentration above the saturation limit produces a supersaturated solution. You can also heat a solid above the equilibrium melting point and produce a superheated solid.
The rate of phase separation depends on two factors:
DG and kinetics. Kinetics slows exponentially at lower temperatures D ~ exp(K/(T-T0)). The thermodynamic driving force, exp(-DG/kT), decays at higher temperatures, so a maximum in growth rate results below the equilibrium in the super cooled liquid state.

## Slide 3
Supercool/Superheat/Supersaturate
The rate of phase separation depends on two factors:
DG and kinetics. Kinetics slows exponentially at lower temperatures D ~ exp(K/(T-T0)). The thermodynamic driving force, exp(-DG(T)/kT), decays at higher temperatures, so a maximum in growth rate results below the equilibrium in the super cooled liquid state.
To homogeneously form a crystal, you need to 1) form a nucleus or seed then 2) grow from the seed. At deep quench you get a lot of seeds but slow growth since transport is slow. At high temperature you see few seeds, but the kinetics are fast.

## Slide 4
Kauzmann Paradox,
a thermodynamic basis for the glass transition
The entropy of the liquid becomes smaller than the entropy of the solid at the Kauzmann temperature, TK. This could be the infinite cooling glass transition temperature.
Selenium like sulfur can form chain molecules
Selenium forms a hexagonal crystal of helical chains (slow kinetics)

## Slide 5
Superheating and Melting
Superheating can occur since melting occurs at surfaces and if the surfaces are stabilized then superheated solids can be produced
Growth of a liquid phase relies on growth of a mechanical instability
A mechanical instability will not spontaneously grow if it occurs in a meta-stable region in T and P:
(dG/dx)=0 defines equilibrium or binodal; (d2G/dx2) = 0 defines the metastable limit or spinodal
(d3G/dx3) = 0 defines the critical point
dG = -SdT + Vdp
Metastable region defined by
(d2G/dp2)T = (dV/dp)T < 0 and (d2G/dT2)p = -(dS/dT)p < 0
First requires that the bulk modulus be positive,
Second requires positive heat capacity, (dS/dT)p = Cp/T > 0
Shear modulus goes to 0 at highest possible supercritical solid
-S U V
H A
-p G T
933K = Tm,Al

## Slide 6
Thermal (energy) fluctuations are the basis of thermodynamics
Map of energy in 3d space at one time slice
https://upload.wikimedia.org/wikipedia/commons/2/2a/Quantum_Fluctuations.gif
Thermodynamic Hypothesis:
Systems are always probing free energy space (temperature, composition, pressure, magnetic field, electrical field, energy, extent of reaction, etc.) through random fluctuations. This enables the attainment of the lowest free energy at an equilibrium state.
This hypothesis leads to consideration of the partial derivatives of free energy as defining features in free energy space particularly critical points (d3G/dx3=0; d2G/dx2=0; dG/dx=0), equilibrium (binodal) points (dG/dx=0), and spinodal points (d2G/dx2=0).

## Slide 7
The book considers first a reversible chemical reaction A <=> B
Cyclohexane from boat to chair conformation for instance
As temperature changes you can observer a different mix of states, E = kBT ~ 2.5 kJ/mole at RT
But fluctuations allow for 0.1 % boat conformation. At 1073K 30% boat. Probability is exp(-E/kT).
The percent in boat can be measured using NMR spectroscopy.
Chair
Chair
Boat
Transition
State
Metastable
Transition
State
The equilibrium point depends on temperature, kBT

## Slide 8
Extent of reaction would be the conversion from chair (A) to boat (B), for instance, at a temperature T. The minimum, (dG/dx) = 0 is the equilibrium point. The free energy plot can be concave up (stable equilibrium) concave down (unstable), flat (critical point/temperature), and other shapes
A <=> B
Affinity
At temperature T, the reaction is like a spring bouncing between A and B oscillating about the equilibrium point since any deviation from equilibrium increases the free energy.

## Slide 9
Stable dG/dx = 0
Unstable
Spinodal d2G/dx2 = 0
Metastable (This can depend on your vantage point)

## Slide 10
Affinity as a Taylor series in the reaction coordinate
z is a fluctuation in a reaction coordinate, T, p, m, x, etc.
At equilibrium, the affinity is 0 so = 0
If then the equilibrium is stable

## Slide 11
Construction of a Phase Diagram Based on Fluctuations
Consider the Hildebrand Model
Binodal phase equilibria is defined by
xA = 1-xB and d(ln(x)) = dx/x
Spinodal is defined by
Critical Point is defined by
d3Gm/dxB3 = RT(1/(1-xB)2 - 1/xB2) = 0 or xA = xB = 0.5
Using this composition in d2Gm/dxB2 = 0 yields

## Slide 12
Hildebrand Equation

## Slide 13
If W = -A + BT, and the entropy term is small (for polymers for instance) B is non-combinatorial entropy
Phase separation occurs on heating: Lower Critical Solution Temperature (LCST)
Flory-Huggins Equation
fA is the volume fraction of A
NA is the number of “c” units in A
nc is the total number of c volume units in the system
C is an average of A and B units
Volume fraction has replaced mole fraction
is an average interaction energy per c site per RT
~ W/RT
Symmetric blend NA = NB
Entropy part is small since Ni ~ 100,000
c ~ a - b/T leads to LCST behavior, “a” is non-combinatorial entropy, “b” is the enthalpy of specific interactions that leads to miscibility
2 Phase
1 Phase

## Slide 14
Since cN depends on 1/T specifying cN specifies the temperature. Large cN is low tempearature.

## Slide 16
Joon Roe

## Slide 17
Spinodal
B
B

## Slide 18
Spinodal
B
B

## Slide 20
Higgins JS, Cabral JT A Thorny Problem? Spinodal Decomposition in Polymer Blends Macromolecules 53 4137−4140 (2020)

## Slide 21
Free energy density
Series expansion of the free energy density yields,
Positive second derivative leads to increase (Stable)
(Smile up)
Negative to decrease (Phase Separation)
(Frown down)
P. 125 Strobl Chapter 4

## Slide 22
Diffusion in Nucleation and Growth and in Spinodal Decomposition
Fickian diffusion down a concentration gradient
Spinodal diffusion up a concentration gradient driven by free energy

## Slide 23
Diffusion in Nucleation and Growth
P. 127 Strobl Chapter 4
Rate of Nucleation
Free energy Barrier
Homogeneous vs Heterogeneous Nucleation

## Slide 24
Phase grows from fluctuations
Higgins JS, Cabral JT A Thorny Problem? Spinodal Decomposition in Polymer Blends Macromolecules 53 4137−4140 (2020)

## Slide 25
Growth rate at q

## Slide 26
Flory-Huggins with a gradient term

## Slide 27
R(q) can be measured by light scattering
For Polymers
(X-ray or neutron for metals/ceramics)

## Slide 28
Transport
Thermodynamics
Size
(Entropy of the gradient)

## Slide 30
Activation Barrier for Nucleation and Growth
Balance between bulk and surface
Free energies
(Next chapter)
Different relative bulk to surface free energies (small to large)
Rate of Nucleation
Free energy Barrier

## Slide 31
Critical Scattering from Single Phase Polymer Melt (neutron scattering 10Å)
A polymer chain in a melt is a random walk like a diffusion path so Mass ~ size2
By Bragg’s law size is related to inverse angle
d = 2/(l sinq)
Reduced angle is q = 4p/l sinq
Intensity (S) scales with Mass
So, S ~ q-2
Then a plot of 1/S vs q2 should be a line that reflects the inverse of contrast at q = 0
At the critical point contrast goes to ∞ so 1/S goes to 0.
Deuteration provides contrast for neutrons, l = 10Å.

## Slide 32
After a T-jump to the 2-Phase region (Light Scattering 0.6 µm)

## Slide 33
Vycor and Pyrex Glass
Na2B8O13-SiO2

## Slide 34
Vycor
Pure fused silica is difficult to shape
Adding boron trioxide makes the melt more formable
Phase separation in the spinodal region leads to continuous phases
The boron can be leached out using acid leading to 96% silica in a simple process
Pure fused silica is very strong and resists thermal shock due to low thermal expansion coefficient
(High precision lenses)
If the glass is not reheated to remove the pores it can be used as a filter or water absorber
Pyrex
Adding boron trioxide makes the melt more formable and have a lower thermal expansion coefficient (1911).
Phase separation in the binodal region leads to boron domains in a silica matrix. This composition is used for CorellewareTM
2-phase white translucent ceramic

## Slide 35
(dP/dV)T = -(dT/dV)P (dP/dT)V Triple Product Rule
= - (1/a) (a/k) First by def. second from Cp Cv calc.
= -1/k
So, the P vs. V plot must have a negative slope!!
Positive slope part is imaginary
In the immiscible region, changes in V occur by
converting liquid to vapor or vapor to liquid
at constant P so (dP/dV)T = 0 in the 2-phase region.
van der Waals Equation
(isothermal plot)
p = RT/(V-b) – a/V2
= 0

## Slide 36
Is unphysical
Negative compressibility
Common Tangent Method for T/Tc = 0.8
Maxwell equal area construction
P ~ 1/V ideal gas
isothermal
Van der Waals
At Tc, Pc
At the critical point
T/Tc = 1
In two phase region

## Slide 37
P ~ T ideal gas
isobaric
isochoric
Vapor pressure of water

## Slide 38
Polymorphs (compound) and Allotrophs (single element)
Allotroph of a single element: Carbon as diamond or graphite
Polymorph of a compound:
Titania as anatase or rutile
Silica as α-quartz, β-quartz, tridymite, cristobalite, moganite, coesite, and stishovite
Calcium carbonate as calcite or argonite
Ostwald step rule: Least stable polymorph crystallizes first since it has
a free energy that is closest to the liquid or solution state. This means that metastable phases form kinetically first if they exist. If many polymorphs exist, they will form in order of free energy with the highest forming first.
Ostwald’s rule: Most stable polymorph does not always crystallize, rather, meta-stable polymorphs form at a higher rate if the surface tension difference between the melt/liquid solution and the polymorph is small.
Ostwald ripening: Metastable polymorphs may form small crystals. Over time stable polymorphs grow from these small crystals into large crystals. This has been generalized to growth of large phases due to ripening such as in crushed ice or ice cream.
Ostwald-Freundlich Equation: Small crystals dissolve more easily than large crystals. This is the reason for Ostwald ripening. Also true for vapor pressure of a liquid droplet (replace x with p)

## Slide 39
1 Nucleation, 2 diffusion-limited growth, and 3 Ostwald ripening/coalescence.

## Slide 42
Piezoelectric