## Slide 1
Surfaces impact the free energy
It takes energy to form surfaces
Small particles dissolve easier
There are limits to grinding, fine powdered sugar is about 50µm

## Slide 2
Surfaces impact the free energy
It takes energy to form surfaces
Small particles dissolve easier
There are limits to grinding, fine powdered sugar; about 50µm
DH/r3 = DHbr3/r3 + sr2/r3
= DHb + s/r

## Slide 3
Aggregates versus primary particles

## Slide 4
Aggregates versus primary particles
Nitrogen (or Argon) adsorption
Other methods:
SAXS
TEM
SEM
OM
XRD (Scherrer Equation)
Aerosol Methods (DMA)

## Slide 5
Liquid-gas or solid-gas interface is called a surface
For surfaces we define a surface tension, s, energy/area
Liquid/liquid or solid/liquid or solid/solid is just called an interface
For interfaces we define the interfacial energy, g, energy/area
Gibbs Surface

## Slide 6
Surface Excess Moles
The adsorption of “i”
There could be surface excess “i” or surface depletion of “i”
Gi can be positive or negative
Surface Excess Properties
Adsorption (not Absorption) see video
Adsorption of i
Surface Excess Gi

## Slide 7
Surface Excess
-SUV
H A
-pGT
V doesn’t change
Surface excess
What is the change in internal energy by introduction of a surface?

## Slide 8
If the thickness is much smaller than r you can ignore curvature
1) Surface Area and 2) Curvature Energy Terms, cx = 1/rx, cy = 1/ry
Surface Tension
Definition of
Surface Tension
For V/L or V/S
Two additional contributions to the surface energy
Enthalpic Term

## Slide 9
dl
Curved Interface (Laplace Equation psat ~ s/r)
Pressure reaches equilibrium
a
b
a
b
dl
dAs = 0 for flat surface
For a sphere A =4p/3 r2 :: dA =8p/3 r dr
c = 1/r so dA = 2A/r dr = 2Acdr
if dr = dl dA = 2cAdl
Change in internal energy is proportional to the change in interfacial width
Derive Laplace Equation
Force/Area x Distance = Energy/Area

## Slide 10
Laplace Equation
For a 100 nm (1e-5 cm) droplet of water in air (72 e-7 J/cm2 or 7.2 Pa-cm)
Pressure is 720 MPa (7,200 Atmospheres)

## Slide 11
Solid interface in a 1-component system
Work to create the interface
Interfacial energy, g
Surface creation always has an energy penalty.
is always positive
Nano-particles are unstable (increase in free energy with a surface)
Differences in surface energy for different crystal surfaces leads to fibrous or lamellar crystals
-SUV
H A
-pGT
For S/S, S/L, L/L

## Slide 12
Crystal surface energy ~ number of bonds * bond energy
Density of bonds decreases with Miller Indices
FCC Nearest Neighbors Number of bonds
[111] 6 3
[110] 12 6
[100] 8 4
Liquid droplets minimize surface area for a given volume
So, Spheres form
At high temperatures crystalline solids also form spheres
Because surface energy becomes less important
Consider a crystal with constant volume with N facets.
Draw a vector from the center of a crystal to a face, hn.
(Each pair share a bond)
Gibbs-Wulff Theorem

## Slide 13
Wulff Construction
Surface excess energy
Draw a vector from the center of a crystal to a face.
Gibbs-Wulff Theorem states that the length of the vector is proportional to the surface energy
hj = l gj
Minimization to find the lowest free energy
hj Oj is proportional to the volume of a facet so for constant volume:
And for constant volume:
And
So:
And
Diffusion rates and twinning can alter the crystal shape for large crystals
Higher energy surfaces grow preferentially (l is a constant)
O is area
g surface energy

## Slide 14
Pressure difference for solid crystal facets
(Force/length)/length = Force/Area
Laplace Equation
Isothermal
Equilibrium
gdA/V = 2gd(1/h) = -dp

## Slide 15
Strength of bonding impacts surface tension
d-block transition metals have strong bonds

## Slide 16
Strength of bonding impacts surface tension
d-block transition metals have strong bonds

## Slide 17
Strength of bonding impacts surface tension
d-block transition metals have strong bonds

## Slide 19
Empirical relationship for the temperature dependence, entropy at interface is high, n ~ 1.2 for metals.
For a liquid with its own vapor
Reminiscent of DG = DH(1-T/T*)
Liquid/Vapor surface

## Slide 20
From Hiemenz’s Book
Force to increase a 2d film area
You apply the force to the the side l and the opposite side l so 2l. F ~ 2l or F/(2l) = g

## Slide 21
w = Force
P = Wetted Perimeter
t = Thickness
l = Plate Length
Perimeter gamma cosq= mgh
Jurin’s Law

## Slide 22
Jurin’s Law
1) Atmospheric Pressure above, Liquid pressure below
Laplace law indicates
Dp = 2s/r where r is r0/cosq if the meniscus is circular
2) Pressure in the tube follows p = p0 - rgh where p0 is atmospheric pressure (hydrostatic pressure)
3) At equilibrium rgh = 2s cosq / r0
So, h = 2s cosq /(rg r0)

## Slide 23
Young-Dupré Equation

## Slide 24
Young-Dupre Equation

## Slide 25
t is the tangent vector along the surface at the point of contact, ts is a force in the tangent direction
Larger angle means smaller displacement t, t ~ 1/sin(q)
This defines the observed angles in a micrograph in terms of the surface tension for the various phases
Law of sines

## Slide 26
Three phases and three angles
Define the phase by the angle
Take the a, q line as the vector direction then
gaq + gqbcos(q) + gbacos(a) = 0 using the dot product of the vectors
For the q, b line as the vector direction then
gaqcos(q) + gqb + gabcos(b) = 0 using the dot product of the vectors
For the a, b line as the vector direction then
gaqcos(a) + gqbcos(b) + gab = 0 using the dot product of the vectors
b is a flat rigid surface, b = p
gaqcos(q) + gqb + gabcos(b) = 0
gglcos(q) + gls - ggs = 0
Spreading Parameter: S>0 wets; S<0 partially wets
For S<0
3 equations and
3 unknowns
You can solve for three interfacial tensions

## Slide 27
Dihedral Angle

## Slide 28
Dihedral Angle in Microscopy

## Slide 29
Pressure for equilibrium of a liquid droplet of size ”r”
Reversible equilibrium
At constant temperature
dpl =Vg/Vl dpg
Differential Laplace equation
Small drops evaporate, large drops grow
Large excursions away form the equilibrium pressure makes nanoparticles (deep quench far from equilibrium)
How do you make small particles? (Nanoparticles)
-SUV
H A
-pGT

## Slide 30
In the absence of nuclei, the initial bubbles on boiling can be very small
These bubbles are unstable due to high pressure so boiling can be prevented leading to a superheated fluid
Equilibrium
Ideal gas
Laplace equation for pressure
Smaller bubbles at higher temperatures
(Far from equilibrium)
-SUV
H A
-pGT
Initial Bubbles on Boiling

## Slide 31
Solubility and Size, r
Consider a particle of size ri in a solution of concentration xi with activity ai
Derivative form of the Laplace equation
Dynamic equilibrium
For an incompressible solid phase
Definition of activity
Solubility increases exponentially with reduction in size, r
(xil)r = (xil)r=∞ exp(2gsl/(rRT r))
Small particles dissolve to build large particles with lower solubility
-To obtain nanoparticles you need to supersaturate to a high concentration (far from equilibrium).
-Low surface energy favors nanoparticles. (Such as at high temperatures)
-High temperature and high solid density favor nanoparticles.
Supersaturation is required for any nucleation
-SUV
H A
-pGT
One form of the Gibbs-Thompson Equation
Ostwald-Freundlich Equation

## Slide 32
Ostwald Ripening
Dissolution/precipitation mechanism for grain growth
Consider small and large grains in contact with a solution
Grain Growth and Elimination of Pores
PV = m

## Slide 33
Critical Nucleus and Activation Energy for Crystalline Nucleation (Gibbs)
(M/r) is molar volume
Surface increases free energy
Bulk decreases free energy
Barrier energy for nucleation at the critical nucleus size beyond which growth is spontaneous

## Slide 34
Critical Nucleus and Activation Energy for Crystalline Nucleation (Gibbs)

## Slide 35
Critical Nucleus and Activation Energy for Crystalline Nucleation (Gibbs)
DfusGm = DfusHm - TDfusSm
Lower T leads to larger DfusGm (Driving force for crystallization)
smaller r* and smaller Dl-sG*
Deep quench, far from equilibrium leads to nanoparticles
One form of the Gibbs-Thompson Equation

## Slide 36
Third form of the Gibbs-Thompson Equation
Third form of GT Equation/ Hoffman-Lauritzen Equation
B is a geometric factor from 2 to 6
Crystallize from a melt, so supersaturate by a deep quench
Free energy of a crystal formed at supercooled temperature T
At equilibrium for an infinite crystal (r = ∞) Df = 0 = DH – TDS so DS = DH/T∞
For a small crystal of size “r” at “equilibrium”
r = BgT∞/(DH(T∞-T))
Small particles at deep quench

## Slide 37
Heterogeneous versus Homogeneous Nucleation

## Slide 38
Formation of a surface nucleus versus a bulk nucleus from n monomers
Homogeneous
Heterogeneous (Surface Patch)
Surface energy from the sides of the patch
Bulk vs n-mer
So, surface excess chemical potential

## Slide 39
Barrier is half the height for surface nucleation
Stable size is half the size

## Slide 40
Adamson Physical Chemistry of Surfaces pp. 328 Classical Nucleation Theory

## Slide 41
condensation

## Slide 42
Growth rate I is related to collisions Z and Boltzmann probability

## Slide 44
Three forms of the Gibbs-Thompson Equation
Ostwald-Freundlich Equation
x = supersaturated mole fraction
x∞ = equilibrium mole fraction
n1 = the molar volume
Free energy of formation for an n-mer nanoparticle from a supersaturated solution at T
Difference in chemical potential between a monomer in supersaturated conditions and equilibrium with the particle of size r
At equilibrium
For a sphere

## Slide 45
Three forms of the Gibbs-Thompson Equation
Ostwald-Freundlich Equation
Areas of sharp curvature nucleate and grow to fill in. Curvature k = 1/r
Second Form of GT Equation

## Slide 46
Three forms of the Gibbs-Thompson Equation
Third form of GT Equation/ Hoffman-Lauritzen Equation
B is a geometric factor from 2 to 6
Crystallize from a melt, so supersaturate by a deep quench
Free energy of a crystal formed at supercooled temperature T

## Slide 47
Nitrogen (or Argon) adsorption

## Slide 48
Langmuir Equation (Wikipedia)
Can be obtained using Equilibria or Kinetic Model
The surface containing the adsorbing sites is a perfectly flat plane with no corrugations (assume the surface is homogeneous). However, chemically heterogeneous surfaces can be considered to be homogeneous if the adsorbate is bound to only one type of functional groups on the surface.
The adsorbing gas adsorbs into an immobile state.
All sites are energetically equivalent, and the energy of adsorption is equal for all sites.
Each site can hold at most one molecule of A (mono-layer coverage only).
No (or ideal) interactions between adsorbate molecules on adjacent sites. When the interactions are ideal, the energy of side-to-side interactions is equal for all sites regardless of the surface occupancy.

## Slide 49
Langmuir Equation (Wikipedia)
Equilibrium Reaction Model
Can be obtained using Equilibria or Kinetic Model
Solvent = 1; Solute = 2; s = surface bound; b = bulk solution free
a1b ~ 1

## Slide 50
Langmuir Equation (Wikipedia)
Kinetic Reaction Model
Can be obtained using Equilibria or Kinetic Model

## Slide 51
Langmuir Equation (Wikipedia)
Kinetic Reaction Model
Can be obtained using Equilibria or Kinetic Model

## Slide 53
Adsorption, Surface Area and Porosity

## Slide 54
(P/P0)/(vads(1-P/P0)) = 1/(Keqvmono ads) + (P/P0)(Keq - 1)/(Keqvmono ads)
1938 Stephen Brunauer, Paul Emmett, and Edward Teller

## Slide 55
Langmuir
BET

## Slide 56
Empirical power-law equation for adsorption

## Slide 57
Adsorption, Surface Area and Porosity

## Slide 58
Adsorption, Surface Area and Porosity

## Slide 59
Surface Energy Term and Block Co-Polymers
Micro-Phase Separation

## Slide 60
How can you predict the phase size? (Meier and Helfand Theory)
Consider lamellar micro-phase separation.
For a symmetric binary blend of polymers, the Flory Huggins equation predicts a critical point at cN = 2.
If the same two polymers are bonded, they microphase separate at cN = 10.5, the bonding makes the polymers more miscible.
Enthalpy associated with phase segregation
Entropy associated with locating the junction points at the phase interface
Entropy associated with stretching the chains
Drives a positive enthalpic contribution that favors micro-phase separation
Assume transition from perfectly mixed to perfectly demixed
An interfacial layer of thickness dt, Area per polymer chain op

## Slide 61
dA
dB
dt
R02 = Nl2
R = b dAB = b(dA + dB)
How can you predict the phase size? (Meier and Helfand Theory)
Consider lamellar micro-phase separation.
For a symmetric binary blend of polymers, the Flory Huggins equation predicts a critical point at cN = 2.
If the same two polymers are bonded, they microphase separate at cN = 10.5, the bonding makes the polymers more miscible.

## Slide 62
dA
dB
dt
There is only one free parameter, for instance op,
the cross-sectional area per polymer chain (Tom Witten, U Chicago)
Find the minimum in the free energy by varying op
Ignoring “ln” term that varies slowly
How can you predict the phase size? (Meier and Helfand Theory)
Consider lamellar micro-phase separation.
For a symmetric binary blend of polymers, the Flory Huggins equation predicts a critical point at cN = 2.
If the same two polymers are bonded, they microphase separate at cN = 10.5, the bonding makes the polymers more miscible.

## Slide 63
How can you predict the phase size? (Meier and Helfand Theory)
Consider lamellar micro-phase separation.
dA
dB
dt
Perfect match

## Slide 64
Binary Correlation Function (Radial Distribution Function) and S/V ratio
g(r) is the probability of finding a point “x” (diamond) in a phase and
of finding a point “y” (circle) a distance “r” from “x” also in the phase
Consider small “r” compared to the particle size for a smooth/sharp interface (not a spinodal or diffuse interface)
Probability of “x” being in the phase is the volume fraction “f” of the particle phase.
There are three possibilities:
r
Yes
No
No
Volume
Surface
Yes for “x” = f
g(r) = Yes for “x” and for “y” = f (1 – (S/V) r)
So, this is a straight line that decays with (S/V)
For small “r” where the curvature of the phase doesn’t matter and
For smooth sharp interfaces, not diffuse and not rough interfaces
The Fourier transform of the correlation function is the X-ray or neutron scattering and small sizes are at large angles in the small angle regime for nanoparticles. The transform of this linear decay is a power-law decay of -4 slope, I(q) ~ S/V q-4 Porod’s Law

## Slide 66
For fine grain particles at times a high Gibbs free energy polymorph forms
S/V ~ 1/r
135 m2/g ~ 12 nm particles
a-Al2O3 is the stable form but g-Al2O3 forms for small particles
g-Al2O3 has a lower surface energy

## Slide 67
Adsorption (Adherence to surface, can be chemical or physical)
Physical adsorption: Low enthalpy of adsorption; reversible adsorption isotherm
Chemical adsorption: Large enthalpy of adsorption; irreversible; chemical change to surface
Hysteresis in adsorption isotherm
Adsorbent
Adsorbate
Solid or Liquid
Molecules in a Liquid or Gas
Surface Excess Moles
The adsorption

## Slide 68
Adsorption, Surface Area and Porosity

## Slide 69
Internal Energy of System:
Surface Excess Internal Energy:
Differential Form with respect to the area:
Subtract the total derivative from the differential form yields the Gibbs-Duhem for Surface Excess:
-SUV
H A
-pGT
Gibbs Adsorption Equation
Gibbs Adsorption Equation

## Slide 70
Gibbs Adsorption Equation
Gibbs-Duhem Equation:
ds/dln(xB))T = -RT[GB – (xA/xB) GA)

## Slide 71
Relative Adsorption, doesn’t
Va is the volume of the a-phase
Relative Adsorption
Adsorption, G, depends on the position of the “surface”
Multiply second equation by c ratio then subtract, it doesn’t depend on the position of the surface.

## Slide 72
Relative Adsorption
Gibbs Surface S is located where there is no net adsorption of A

## Slide 73
Solutes that reduce the surface tension are adsorbed

## Slide 74
For an ideal gas µB = RTlnpB where pB is the partial pressure of B
Surface Activity of B
Henry’s Law for Surfaces (surface impurities change surface tension)
At infinite dilution so Henry’s Law Regime
A small number of electronegative elements can have a large impact on surface energy of metals jA ~1000 for oxygen and sulfur
Define j as the surface activity of an impurity