Quiz DMTA

- Make a sketch of the general design of a dynamic mechanical thermal analysis instrument (DMTA).

- How does a DMTA compare with a dynamic dielectric spectrometer?

- How are the loss and storage modulus and tan δ determined using the DMTA?

- What is a Cole-Cole Plot?  How should this plot look for a material with a single relaxation time?

- Sketch the storage, loss modulus and tan δ for a semi-crystalline polymer across temperatures covering the glass, glass transition temperature, rubbery plateau, and melting point.

- What is the WLF equation?  How does it differ from a simple Arrhenius behavior and from Vogel-Fulcher behavior?

- How can the WLF equation be used to shift DMTA data from different temperatures to a master curve as a function of frequency?

- Explain why and for what samples you might want to use the following types of deformation in a DMTA:  Tensile, Compressive, Shear, 3 Point Bend, Torsion.

- What is the expected effect of adding a filler on time-temperature superposition?  (For example in a tire.)

- What is the plateau modulus and how can it be used to calculate the entanglement molecular weight?

- What information can be obtained from a Cole-Cole plot from DMA data other than if the materials displays a single relaxation time.