## Slide 1
Sandip Argekar
Specular reflectivity – Examples and applications

## Slide 2
Specular reflectivity
Quantitative information of thickness and SLD in Z direction
Ѳrefl=Ѳincident
Footprint, Critical angle
q-4 decay, roughness
7 to 8 orders of magnitude drop in intensity
Background

## Slide 3
Features - Footprint effect
Low q
High q
In the regime of total external reflection, some intensity is lost as the footprint on the surface is too large
Foot print depends on beam width & sample geometry

## Slide 4
Critical edge
The refractive index for x-rays and neutrons in materials is less than 1.
Total external reflection occurs

## Slide 5
2 critical edges observed
Double critical edge – Better guestimation of layer SLD

## Slide 6
Smooth surface
Rough surface
Maximum specular reflection
Increased non-specular reflection
Loss of intensity and sharpness
Effect of roughness depends on coherence length lc
Only If roughness features < , reflectivity profile is affected
Effect of roughness on the reflectivity profile

## Slide 7
X-ray reflectivity single layered system
Kiessig fringes
Fringes with uniform spacing
Thickness of the layer :
SLD of the layer pushes the curve up or down

## Slide 8
7 crests
Multilayered systems – PS 19
Identify critical edge
  Calculate substrate SLD
Guess number of layers
  Based on practical expt
  Calculate approx SLD
Guess preliminary thickness

## Slide 9: Neutron reflectivity
Utilize contrast between H and D to understand polymeric and biological systems
Swelling studies under dueterated solvents
D2O
Si
Liquid cell configuration
Neutrons penetrate through Si
D2O becomes the new substrate
For Neutrons

## Slide 10
Courtesy - Peng Wang presentation

## Slide 11
Temperature dependent swelling of poly (N-isopropylacrylamide)
Swelling of a hydrogenated polymer with D2O
Water penetration shows a diffuse profile
Non-swollen polymer at the substrate interface
Diffuse layer
Critical temperature

## Slide 12
Panalytical XRD pro MD setup – X-ray reflectivity – Goniometer based
LANSCE –SPEAR - Neutron reflectivity – Time of flight approach

## Slide 13
http://www.ncnr.nist.gov/resources/sldcalc.html
Handy tools – SLD calculator

## Slide 14
Handy tools – Reflectivity data fitting Parratt 32