## Slide 1
An Overview of Plastics
to Understand their Problems and Potential

## Slide 29
LPG Alkylation using HF

## Slide 30
Shazand Petrochemical complex

## Slide 31
It is possible to balance the products of oil refining to meet market demand to some extent but there is some connection between the amount of petrochemical fuels used and the amount of olefins produced.
There is a direct link between the price of polyethylene/polypropylene and the price of oil.
If we stop using polyolefins it will have an impact on the petrochemical industry possibly leading to more waste. The petrochemical system is complex.
A more obvious link between plastics and industrial waste streams is Cl2.
OCM Oxidative Coupling of Methane

## Slide 32
NaOH (40g/mole)
HCl (36.5g/mole)
It would appear that without PVC, CPE and other polymers we would have 4,000 M kg extra Cl2
which would be waste
Many polymers are essentially long-term disposal methods
Cl2 (71g/mole)

## Slide 34
Ethane and Propane feed lines to crackers for olefin production
LyondellBasell
Clinton Iowa Polyethylene Plant

## Slide 36
https://www.qcpolymers.com/en/about-the-company/
https://youtu.be/Vrz1h2cwKL0?si=263vUVOwkrPArEMV
https://www.lyondellbasell.com/en/news-events/corporate--financial-news/lyondellbasell-acquires-mechanical-recycling-assets-and-plans-operations-in-california/

## Slide 41
Long chain branching (HDPE)
Short chain branching (LLDPE)
Metallocene PE
LDPE
SBR for tires is anionically polymerized triblock
Pluronics for hand sanitizer is a PEO/PPO block copolymer

## Slide 43
Sulfur vulcanization of polyisoprene (natural rubber)
PDMS silicone rubber crosslinked with TEOS

## Slide 47
21 Common Plastics (the short list)
(Polymers, Rubbers, Thermoset, Thermoplastic, Colloids, Latexes, Adhesives, Lubricants, Coatings, Inks)
PS
Free Radical
Anionic
HIPS
PS Foam
Rigid Plastic
SBR
BCP
Anionic
PET or PETE
Condensation
Bottles, Rugs
PE
Free Radical
Single Site Metallocene
Ziegler-Natta
HDPE,LDPE, LLDPE,
Metallocene
Bags, Jugs,
Climbing Toy
i-PP
Ziegler-Natta
Tough plastic
PI
Natural
Rubber
Anionic
Ziegler-Natta
Polybutadiene
Free Radical
Anionic
PLA
Condensation
Bio sourced
PHB (PHAs)
Random CPs
Bio sourced
PEO or PEG
Ring opening
condensation
PPO
condensation
Pluronic
PEO-PPO
BCP
Ring opening
condensation
PVC CPE
Plasticized Crystalline Polymer
Dashboard
Pipe
Polysulfone
Free radical
Prison
Dishes
Resorcinol-Formaldehyde
Condensation
Electronics
Epoxy ring opening
Condensation
Composites
Polyvinylalcohol
Free Radical
Fibers
Nylon PA
Condensation
Fibers
PDMS ring-opening
Condensation
Rubber
Polyurethane
Condensation
Foam/coatings
Acrylics
Free Radical/Anionic
Plexiglass® PMMA
superabsorbent
Polycarbonate
Condensation
Polyester
CDs, subway
windows

## Slide 48
Some Common Additives
(Pigments, Foaming Agents, Silica, Carbon Black, Titania, Calcium Carbonate, Flame Retardants,
Anti-oxidants, Processing Agents, Lead Stearate, Residual Catalyst, Chromium, Plasticizer, Magnetite,
Ferrite, Glass Fiber, Sizing Agent)

## Slide 49
PS
Free Radical
Anionic
HIPS
PS Foam (EPF)
Rigid Plastic
Ethylene + Benzene over AlCl3 makes ethylbenzene, dehydrogenated by heat makes styrene (1000°C)
A suspension of styrene in water using barium sulfate or polyacrylate as a suspension agent. Water cools the reaction, and the product is a suspension of PS beads.

## Slide 51
Gel Permeation Chromatography (GPC) or High-Pressure Liquid Chromatography (HPLC)
-About 50 MPa pressure.
-Flow rate is very slow, 1-2 ml/min
So, molecules have time to explore the gel matrix by lateral diffusion
-The gel matrix is a mass-fractal network, so the volume explored goes as 1/(the size of the probe molecule)df where df is the mass fractal dimension from 1 to 3 typically 2.5 for a random network.
-Small molecules explore a much larger volume, so they spend a lot longer in the column and have a larger “elution volume”
-Branched chains are smaller than linear chains of the same molecular weight

## Slide 53
SBR
BCP
Anionic

## Slide 56
ABS
Tertiary CP
Anionic Polymerization
Processing/mixing

## Slide 58
HIPS
Free Radical
Free radical polymerization of a mixture of the monomers. PBD initially polymerizes as the majority phase, styrene polymerizing later. A phase inversion occurs where the polystyrene becomes the matrix phase with inclusions of polybutadiene that have polystyrene drops within the rubber. The process is dependent on vigorous mixing during polymerization. The two components are immiscible.
Dixie cup

## Slide 59
Colloidal PS
Emulsion Polymerization
Latex paint
Water, Monomer (oil), Surfactant
Polymerization in the Latex/Colloidal particles
Latex Paint, colloidal polystyrene (monodisperse spherical particles)
Exfoliants in cosmetics

## Slide 66
https://en.wikipedia.org/wiki/File:Plastic_Injection_Molding.webm

## Slide 67
Polystyrene Foam
Residual Styrene
Hexane
CFC
Blowing Agents

## Slide 68
PS
HIPS (Crazing)
ABS (Shear Banding)

## Slide 69
PET or PETE
Condensation
Bottles, Rugs
In “bio-PET” the ethylene glycol is derived from sugar fermentation.

## Slide 70
Polyethylene
PET
“Prepolymer”
“Polymerization”
Multi reaction vessels

## Slide 73
Polycarbonate
Condensation
Polyester
CDs, subway
windows

## Slide 74
Polycarbonate
Condensation
Polyester
CDs, subway
windows
https://www.youtube.com/watch?v=O3FQzwNzUE4

## Slide 75
Blow Molding

## Slide 88
PE
Free Radical
Single Site Metallocene
Ziegler-Natta
HDPE,LDPE, LLDPE,
Metallocene
Bags, Jugs,
Climbing Toy
Initiation
Propagation
Ziegler-Natta Catalyst for i-PP and HDPE

## Slide 89
Termination

## Slide 90
Phillips Chromium Catalyst
HDPE

## Slide 91
High Pressure Polymerization for LDPE
1000-3000 Atm (250 MPa)
150-300°C
Supercritical Ethylene
Tc = 9.5°C Pc = 5.06 Mpa
Originally in Autoclave,
Later in Tubular Reactor
And in combination of Autoclave and Tubular
Tube has lower surface area so can withstand more pressure
i.e. safer
Tube has better heat transfer to remove heat from reaction
Short Chain Branching
(Back biting)
Long Chain Branching
(Chain Transfer)

## Slide 92
Metallocene Catalysts

## Slide 93
https://www.pslc.ws/mactest/mcene.htm#pol
This can lead to controlled structure and tacticity due to the steric effects at the active site
i.e. rubbery PE or blocky tactic PP

## Slide 95
HDPE has ”long chain branches” about 1/10,000 which can increase the melt viscosity by a factor of 8
LDPE has arboreal branching or branch on branch structure
LLDPE Does no have arboreal branching but has controlled short chain branching that reduces the degree of crystallinity (DOC)

## Slide 96
Ultra-high Molecular weight Polyethylene (UHMWPE)
Typically, molecular weight is about 80,000 g/mole for HDPE/LDPE/LLDPE
UHMWPE is about 5,000,000 g/mole (20 times normal PE)
It can’t be melt processed so it is processed in rotational molding to make things like truck bed liners and coal shoots and cups for hip implants
It has great wear resistance and doesn’t make microplastics during wear but very difficult to process
Gel-spinning leads to ultra oriented polyethylene which is used for racing sails and bullet proof vests.
Space Tether, Space Elevator, Skyhook

## Slide 97
Blown Film

## Slide 98
Cast Film

## Slide 99
Wire Coating

## Slide 100
Rotational Molding

## Slide 101
Multi Layer Blow Molding

## Slide 102
i-PP
Ziegler-Natta
Metallocene
Tough plastic
Gas phase, Fluidized bed of catalyst
Slurry Reactor, Alkane solvent and propylene gas passed through slurry
Bulk polymerization, 30-40 atm 60-80°C (sub critical Pc = 45 atm, Tc = 92.2 °C)

## Slide 103
i-PP from Ziegler-Natta Polymerization

## Slide 104
PVC CPE
Plasticized Crystalline Polymer
Dashboard
Pipe
80% Suspension Polymerization
12% Emulsion Polymerization
8% Bulk Polymerization
Dibutyl Pthalate Plasticizer

## Slide 105
Chlorinated PE
Aqueous suspension of PE powder with Cl2 gas added

## Slide 106
Nylon PA
Condensation
Fibers
Hexanedioic acid

## Slide 107
https://youtu.be/4GxeSO7DyaE
Peptide Bond

## Slide 108
Peptide Bond
https://youtu.be/cn6K1m7yH0I
Polymer melt spinning

## Slide 109
PI
Natural
Rubber
Vulcanize
Anionic Polymerization
or Ziegler-Natta
Natural
Rubber

## Slide 110
PLA
Condensation
Bio sourced
Lactic acid is produced by fermentation of organics

## Slide 111
PHB (PHAs)
Random CPs
Bio sourced
PHB is directly produced by fermentation
Can be transgenically grown in soybean and other crops

## Slide 112
Epoxy ring opening
Condensation
Composites

## Slide 113
Resorcinol-Formaldehyde
Condensation
Electronics
Plywood

## Slide 114
Polyurethane
Condensation
Foam/coatings
Condensation polymer with no condensate

## Slide 115
PDMS ring-opening
Condensation
Rubber