## Slide 1
Plastics Packaging
120 million metric tons of plastic in packaging per year globally
60% of plastics found on beaches
Monolayer Film:
Plastic Wrap
Shopping Bags
Multi-layer Film:
Pouches and Sachets

## Slide 2
Ideal Packaging:
Protect product from breakage, spoilage, contamination
Extend shelf-life/usage-life
Safeguard hygiene
Attractable appearance
Minimal material usage
Reduce package size
Reduce weight
Packability
Multiuse
Barrier properties tuned to product
Recyclability/Reuse/Downcyclability/Upcyclability?

## Slide 4
Flexible Packaging:
Usually multilayer
bulk layers (outer)
barrier layers
tie layers
heat sealable layers

## Slide 10
Biaxially Oriented Polypropylene Film

## Slide 11
Biaxially Oriented Polypropylene Film

## Slide 16
Higher ethylene has lower barrier but lower temp processing

## Slide 27
Fat content
MW substance
Film Thickness

## Slide 28
Forms of Flexible Packaging
T-shirt bag
Wave-top bag
Soft-loop handle bag
Die cut handle bag
Shrink wrap (LDPE), stretch wrap (LLDPE) , bubble wrap (LDPE), twist wrap (iPP multilayer)
Stand-up pouches SUP
PET, BOPP, nylon, PE,
tie layers, aluminized
or foil
Lay flat/pillow pouches
LDPE, HDPE
LDPE, HDPE, iPP

## Slide 29
Forms of Flexible Packaging

## Slide 30
Labels and Sleeves
iPP, OPP, glycol-modified PET (PET-G), LDPE, PVC, PS.
PET-G Shrink wrap label and sleeves for PET containers
Polymer made of the same material as the container or film do not act as further contaminates and can be recycled with the film or container. e.g. OPP label on HDPE or PP bottles

## Slide 35
Straps/Tapes/Six-Pack Rings
Straps and Tapes: Thin, flat plastic bands PP or PET
6-Pack Rings are LDPE
None are recyclable

## Slide 36
Woven Bags/Net Bags/Sacks
HDPE, PP, PET, Nylon
BOPP
For industrial materials, the bags are recycled

## Slide 37
Coated/Printed Film
PVDC, improves barrier for transparent films
Printing:
Flexographic-
UV or IR cure
Printed or coated film can be recycled for trash bags coating can’t be removed.

## Slide 38
Rotogravure-
Digital-

## Slide 39
Applications of Flexible Packaging
Food and beverage-
Largest Segment
Multilayer films with Aluminum foil and Polyolefins or PET/polyamide
Coating with PVDC to improve O2 barrier
Heat sealing material like wax

## Slide 40
Cleaning Products-
Soap wrappers
Laundry detergent pods (polyvinyl alcohol PVOH)
Liquid detergent pouches
Hand soap tubes
powder soap pouches
Dishwasher pouches
Dishwasher pods
Pouch packing for cleaning chemicals

## Slide 41
Medical/Personal Care/Cosmetics
Printed Aluminum Layer
Forming Film
LDPE, LLDPE, BOPP, OPP, PET, polyamide, PVC, PVDC
Considered medical waste

## Slide 42
Flexible Pouches for Infusion
-Zero volume chamber
-Retained asepsis
-Reduce waste
PVC or polypropylene

## Slide 47
Construction and Building
Stretch Film made of LLDPE
Bricks,
Tiling,
Roofing
Truss structures
Woven PP bags
For sand
Bricks
Cement
PP or PET straps for
Ceramic tile pavers
Building blocks
Recycling is common

## Slide 48
E-Commerce
20% of retail sales
Layers of LDPE and HDPE
Usually not for curbside recycling
Labels need to be removed or cut out

## Slide 51
Plastics Packaging
Uses less material, less expensive,
Can be designed to be more appealing,
Printable, rigid packaging needs labels often made of flexible packaging
Tunable transport properties minimize material use

## Slide 52
Recycling and Flexible Packaging

## Slide 53
Recycling and Flexible Packaging
Automated sorting, requires equipment
Sorted material must be shredded to produce flake scrap material
Flake must be pelletized
For rotational molding, spray coating pellets are ground to a powder
Sorting is the main cost and results in material more expensive than virgin resin
80% of flexible packaging are contaminated with food at 10 to 20% of the weight
Packaging films tangle and clog sorting equipment at material recovery facilities

## Slide 54
Recycling Multilayer Flexible Packaging
There is no technology for recycling of multilayer flexible packaging or metallized films
Printing ink, labels, metallized material, adhesives, coatings must be removed

## Slide 55
Recycling Multilayer Flexible Packaging
Each layer (there could be up to 10 layers) must be
Separated
Analyzed and categorized
Recycled (shredded, pelletized)

## Slide 56
Collection of Flexible Packaging
Flexible packaging recycle rate is cited at 2% by some, 3% by others and up to 20% by still others
-Not widely collected around the world
Sources:
Post-consumer
Post-commercial
Post-industrial
Post-consumer:
LDPE, LLDPE, HDPE, iPP and multilayer films
Much of it contaminated with organics and labels/printing
TerraCycle Zero Waste Bags
If you put your recycle in a plastic garbage bag it is removed from the stream at the MRF and sent to landfill

## Slide 57
Collection of Flexible Packaging
EU Rules, originally 2025 then Dec 2025 now 2030…

## Slide 58
Collection of Flexible Packaging
https://www.hefty.com/hefty-renew-starter-kit

## Slide 59
Collection of Flexible Packaging

## Slide 60
Collection of Flexible Packaging

## Slide 61
Collection of Flexible Packaging

## Slide 63
Post Commercial Flexible Packaging Collection
Polyethylene clear film
Large commercial generators
clear bags, stretch wrap film
Doesn’t need to be washed
21% recycling rate
Recycled into trash bags and thicker commercial films
Polyethyelene post commercial mixed color film
Stretch wrap
Polypropylene woven bags

## Slide 64
Postindustrial Flexible Packaging

## Slide 67
Separation and Sorting and Volume Reduction

## Slide 68
Separation and Sorting and Volume Reduction
Materials Recovery Facility (MFR)
separate
densify
Ship to reprocessors or recyclers
Clean MFR works with separated materials
Dirty MRF works with comingled wastes including organic matter
Contamination is a big problem
metals
paper
other plastics
odd objects, batteries, metal parts, etc
Generally flexible plastic films are a contaminant
Plastics Recovery Facility (PRF)
Plastics specific MRF
These don’t exist in the US

## Slide 69
Separation and Sorting and Volume Reduction
Manual and
Vacuum Sorting
Feeds into a bale press
Or film screw

## Slide 70
Air Separators

## Slide 71
Air Separators

## Slide 72
Screens
Ballistic screen
Disc screen
Vibrating screen
Trommel screen

## Slide 73
Grabbers
Hooks grab bags

## Slide 77
Labeling Systems

## Slide 78
Optical Sorters
Visible light (VIS)
high speed camera and light sensors to detect
Doesn’t detect chemical makeup
Near-infrared (NIR)
Use IR fingerprint
Doesn’t detect color
Neither work well with carbon black

## Slide 79
Fluorescent Light
Add Fluorescent material for identification and separation of plastics
Could separate food contaminated films
Doesn’t seem to be used anyplace

## Slide 80
Robotic Sorters

## Slide 82
Eddy Current Separators
Remove nonferrous metals
Aluminum, brass, copper
Rotating magnet create “eddy currents”
“eddy currents” cause metal to be repulsed by the magnetic field and ejected from waste stream.
These can remove aluminized multilayered films

## Slide 84
Volume Reduction
Compactors

## Slide 85
Compactors

## Slide 86
Life Cycle Analysis of Flexible Packaging is Favorable
Flexible film packaging typically results in less
global warming potential,
energy use, and
volume/quantity landfilled
than recyclable rigid package alternatives [21].
21. Reclay StewardEdge. Product stewardship solutions, resource recovery systems, Moore Recycling Associates Inc. Analysis of flexible film plastics packaging diversion systems - Canadian Plastics Industry Association continuous improvement fund stewardship Ontario. Feb. 2013.
Case studies: coffee; motor oil; baby food; laundry detergent pods; cat litter, beverages
In all cases lower water use, carbon footprint, fossil fuel use, product to package ratio, material to landfill

## Slide 88
For Flexible Packaging
Against Flexible Packaging

## Slide 89
Plastics Packaging
Rethink Packaging, Product, System

## Slide 90
Plastics Packaging

## Slide 91
Plastics Packaging
Recycle
Reuse

## Slide 92
Plastics Packaging
Increased quality and functionality in reuse packaging

## Slide 93
Plastics Packaging
Standardized packaging reduces design/production costs

## Slide 94
Plastics Packaging
Drive sales by brand loyalty through deposit and rewards schemes and personalized products and packaging (mix coke and sprite)

## Slide 95
Plastics Packaging

## Slide 96
Plastics Packaging
Government and business need to be involved

## Slide 97
Plastics Packaging
Use renewable energy to produce H2 to make CH3 and alkanes to make PE PP etc.

## Slide 98
Plastics Packaging

## Slide 99
Plastics Packaging
https://www.youtube.com/watch?v=xmTQA-RNygQ

## Slide 100
Plastics Packaging

## Slide 101
Plastics Packaging

## Slide 102
Plastics Packaging