## Slide 1
Kumar SK, Benicewicz BC, Vaia RA, Winey KI 50th Anniversary Perspective: Are Polymer Nanocompsites Practical for Applications? Macromolecules 50 714-731 (2017).

## Slide 2
So, take an example
You are interested in flame retardancy and have two routes:
Pick a polymer with inherent flame retardancy like Teflon® (thermally stable, low flame propagation)
or polyimides (large char) or polysiloxanes (inorganic components to polymer)
Add a material with high thermal conductivity, high heat capacity, char formation or protection of
char that is formed (and is cheap) like Exfoliated clay works. Silica, titania. Calcium carbonate
(ground up rock) can be effective. Nanoparticles can possibly enhance already flame-retardant polymers.
Flame Retardant Polymer Nanocomposites: An Overview Kumar S(different one), Dhawan R, Shukla SK Macromol. Symp. 407 2200089 (2023).

## Slide 3
Flame Retardant Polymer Nanocomposites: An Overview Kumar S(different one), Dhawan R, Shukla SK Macromol. Symp. 407 2200089 (2023).

## Slide 4
The original nanocomposite
Polydisperse aggregates
Processed under shear
Kinetically mixed
Song, L; Wang, Z; Tang, X.; Chen, L.; Chen, P.; Yuan, Q.; Li, L. Visualizing the Toughening Mechanism of Nanofiller with 3D X-ray Nano-CT: Stress-Induced Phase Separation of Silica Nanofiller and Silicone Polymer Double Networks Macromolecules 50 7249-7257 (2017).
100,000x larger
Objective:
Tear resistance
Static charge dissipation
Notes: In stark contrast the original nanocomposite, an automobile tire, comprises of ~50-100nm non-spherical nanoparticles, generally carbon black and silica. Mixing of nanofillers is achieved by applying mechanical shear resulting in high polydispersity in size. The main objective for using carbon black in a tire, other than structural stability, is to enhance tear strength and ensure static charge dissipation. These two properties are dictated by the micron-mm scale filler networks in the polymer bulk.

## Slide 5
Density of grafted chains
Grafted vs Matrix chain length
50Å
Physics Nanocomposites
Monodisperse colloidal particles
Colloidal Solution cast
Thermally
Dispersed
Kumar, S.K., Jouault, N., Benicewicz, B. and Neely, T., 2013. Nanocomposites with polymer grafted nanoparticles. Macromolecules, 46(9), pp.3199-3214.
Kumar, S.K., Benicewicz, B.C., Vaia, R.A. and Winey, K.I., 2017. 50th anniversary perspective: are polymer nanocomposites practical for applications?. Macromolecules, 50(3), pp.714-731.
Asai, M., Zhao, D. and Kumar, S.K., 2017. Role of grafting mechanism on the polymer coverage and self-assembly of hairy nanoparticles. ACS Nano, 11(7), pp.7028-7035.
Objective:
Enhance miscibility
Well dispersed
Phase separated
Sheets, strings, etc.
Notes: The current state of the art engineered nanocomposites comprise of ~5nm spherical nanoparticles, generally colloidal silica. These nanocomposites are solution cast, thermally dispersed and are monodisperse in size. Aimed at enhancing miscibility of these nanoparticles in the polymer matrix, polymer chains are chemically grafted onto their surface. A great body of work has been and is being currently undertaken to understand how the properties of these nanocomposites be tuned by altering the state of dispersion of the nanoparticles. An elegant phase diagram by Sanat Kumar’s group at Columbia shows that increasing the grafting density on the particles and by varying the graft to matrix chain length different emergent structures can be realized.

## Slide 6
The original nanocomposite
Polydisperse aggregates
Processed under shear
Kinetically mixed
Song, L; Wang, Z; Tang, X.; Chen, L.; Chen, P.; Yuan, Q.; Li, L. Visualizing the Toughening Mechanism of Nanofiller with 3D X-ray Nano-CT: Stress-Induced Phase Separation of Silica Nanofiller and Silicone Polymer Double Networks Macromolecules 50 7249-7257 (2017).
100,000x larger
Objective:
Tear resistance
Static charge dissipation
Notes: In stark contrast the original nanocomposite, an automobile tire, comprises of ~50-100nm non-spherical nanoparticles, generally carbon black and silica. Mixing of nanofillers is achieved by applying mechanical shear resulting in high polydispersity in size. The main objective for using carbon black in a tire, other than structural stability, is to enhance tear strength and ensure static charge dissipation. These two properties are dictated by the micron-mm scale filler networks in the polymer bulk.

## Slide 7
~100nm
L. Pahalagedara, H. Sharma, C.H. Kuo, S. Dharmarathna, A. Joshi, S.L. Suib, A.B. Mhadeshwar, Structure and oxidation activity correlations for carbon blacks and diesel soot, Energy and Fuels. 26 (2012) 6757–6764
Rishi, K., Beaucage, G., Kuppa, V., Mulderig, A., Narayanan, V., McGlasson, A., Rackaitis, M. and Ilavsky, J., 2018. Impact of an emergent hierarchical filler network on nanocomposite dynamics. Macromolecules, 51(20), pp.7893-7904.
Mulderig, A., Beaucage, G., Vogtt, K., Jiang, H. and Kuppa, V., 2017. Quantification of branching in fumed silica. Journal of Aerosol Science, 109, pp.28-37. Beaucage, G. Approximations Leading to a Unified Exponential/Power-Law Approach to Small-Angle Scattering. J. Appl. Crystallogr. 1995, 28, 717−728.
Size
Aggregates of primary particles
Multiscale Hierarchical Structures (Dilute filler content)
primary particles
Graphitic layers
Agglomerates of aggregates
Notes: Spheres are simple objects, in the sense that they are symmetrical, and can be easily characterized. Physicists love spheres. In contrast, nanoparticles such as carbon black, and silica are structurally complex. For one, their exists are structural hierarchy in these fillers that extends over multiple size scales. Under dilute concentrations, we used combined SAXS/USAXS to probe the particle structure. The plot in the center shows the scattered intensity as a function of the scattering vector, which is inversely related to the incident wavelength and directly related to the scattering angle.
For X-rays the incident wavelength is on the order of angstroms so at large scattering angles the crystallographic distances can be probed, for example in XRD. For a fixed wavelength, scattering at smaller angles provides information of larger size. The figure in the middle shows the scattered intensity for carbon black in polybutadiene over 4 decades in size.
Specific features of the plot includes a distinct power law slope, and a corresponding knee region as one goes from right to left. The power law slope provides information about the structure, substructure morphology whereas the knee region provides information about the Rg of these structures.
The versatile unified scattering function combines the morphology and size of hierarchical structures, such that level 0 correponds to the graphitic layer, the sheet like morphology is reflected in the -2 power law slope. (see green curve) Level 1 corresponds to primary particles which could be coarse of fine spheres. These primary particles are sintered into aggregates which are agglomerated.
Although SAXS / TEM are complimentary techniques, TEMs provide only a local measure of the structure whereas this limitation is not observed in SAXS. Where scattering lacks is the visualization of the structure, although this limitation was overcome by the works of Andrew Mulderig in our group. Clearly, the simulated structure based on the Unified scattering fits agrees well with the TEM micrographs

## Slide 8
Multiscale Hierarchical Structures (Dilute)
Precipitated Silica
Carbon coated fumed silica
Notes: This structural hierarchy extending over multiple size scales is also observed for precipitated silica, and fumed silica nanoparticles in SBR matrices. The main differences in the structure is that whereas carbon black has a open, chain like aggregates with fewer branches, fumed silica is highly branched. Precipitated silica on the other hand is more convoluted comprising of compact aggregates with voids.

## Slide 9
Mackay ME, Tuteja A, Duxbury PM, Hawker CJ, Van Horn B, Guan Z, Chen G, Krishnan RS General Strategies for Nanoparticle Dispersion Science 311 1740-173 (2006)
When chains are larger than particles system is “dispersed”
Linear chains are swelled in the presence of nanoparticles, Rg grows with volume fraction NP
Studied C60 (Buckeyballs) in PS; PS NP in PS; and dendritic PE in PS
-4

## Slide 10
Mackay ME, Tuteja A, Duxbury PM, Hawker CJ, Van Horn B, Guan Z, Chen G, Krishnan RS General Strategies for Nanoparticle Dispersion Science 311 1740-173 (2006)
An enthalpic mechanism that arises from nanoparticle packing effects operates at the nanoscale and is necessary in order to understand dispersion in this size regime.
-Polymer blend “Chain insertion enthalpy” = Nc
-”NP insertion enthalpy” = Ac = 4pa2c
-Dispersion depends on processing
-When fp ~ 0 the binodal is defined by
fp ~ exp(-(1+ Nc))
for NP fp ~ exp(-(1+ 4pa2c))
The limit of dispersion of C60 is 2%
so, c ~ ze/kT and e ~ 0.02 eV
Can quench a super-saturated “solution”

## Slide 11
Mackay ME, Tuteja A, Duxbury PM, Hawker CJ, Van Horn B, Guan Z, Chen G, Krishnan RS General Strategies for Nanoparticle Dispersion Science 311 1740-173 (2006)
When chains are larger than particles system is “dispersed”
Linear chains are expanded when in the presence of nanoparticles
Excluded volume (1 + f) predicts (1 + f)1/3

## Slide 12
Mackay ME, Tuteja A, Duxbury PM, Hawker CJ, Van Horn B, Guan Z, Chen G, Krishnan RS General Strategies for Nanoparticle Dispersion Science 311 1740-173 (2006)
When chains are larger than particles system is “dispersed”
For PS NP in dPS a negative c is found (compared to positive for PS in dPS)
Short-range VdW forces between particles only act in the orange region. Polymer/NP interaction acts over the whole surface. So, dispersion is favored. The VdW area (orange) changes with particle size.

## Slide 13
Mackay ME, Tuteja A, Duxbury PM, Hawker CJ, Van Horn B, Guan Z, Chen G, Krishnan RS General Strategies for Nanoparticle Dispersion Science 311 1740-173 (2006)

## Slide 14
First, they can have properties distinct from micron-scale fillers. For example, carbon nanotubes are as stiff as graphite fibers, but are almost an order of magnitude stronger.
Second, nanoscale fillers play the role of small mechanical, optical, and electrical defects. These provide an opportunity for multi- functionality (e.g., scratch-resistant, transparent polymers).
Third, they create a large volume of interfacial polymer with properties different from the bulk, providing an opportunity for tailoring properties.
Schadler LS, Kumar SK, Benicewicz BC, Lewis SL, Harton SE Designed Interfaces in Polymer Nanocomposites: A Fundamental Viewpoint MRS Bulltin 32 335-340 (2007).
Why nanoparticles?

## Slide 15
Polymer wets surface
Polymer de-wets surface

## Slide 16
Lower c means greater “miscibility”
Matrix is infinite molecular weight
Top low graft density, s, bottom high
Larger particles have lower “miscibility”
Three curves
Greater miscibility with longer graft chain length
An effective mean-field interaction (ceff) that arises because of the entropic penalty associated with the interface formed between the brush and the matrix chains.

## Slide 17
Vary matrix MW for 110,000 g/mole grafts of PS on silica in PS
Wetting
De-wetting
Wetting
De-wetting

## Slide 18
Wetting
De-wetting
Wetting
De-wetting
Vary matrix MW for 110,000 g/mole grafts of PS on silica in PS

## Slide 19
Chatterjee T, Jackson A, Krishnamoorti R Hierarchical Structure of Carbon Nanotube Networks JACS 130 6934-6935 (2008).
-4
-2
-4
A
F

## Slide 20
Pedersen, J. S.; Sommer, C. Temperature Dependence of the Virial Coefficients and the Chi Parameter in Semi-Dilute Solutions of PEG. In Scattering Methods and the Properties of Polymer Materials; Springer Berlin Heidelberg: Berlin, Heidelberg, 2005; pp 70–78.
Vogtt, K.; Beaucage, G.; Weaver, M.; Jiang, H. Thermodynamic Stability of Worm-like Micelle Solutions. Soft Matter 2017, 13 (36), 6068–6078.
Jin, Y.; Beaucage, G.; Vogtt, K.; Jiang, H.; Kuppa, V.; Kim, J.; Ilavsky, J.; Rackaitis, M.; Mulderig, A.; Rishi, K.; Narayanan, V. A Pseudo-Thermodynamic Description of Dispersion for Nanocomposites. Polymer (Guildf). 2017, 129, 32–43.
Quantitative measure of nano-dispersion (Mean Field)
Greg Beaucage, University of Cincinnati gbeaucage@gmail.com
Correlation length, x = 2/q*
The rate of decrease in I(q)/f with concentration in this intermediate q-range is an indicator of
how well the filler is dispersed in the elastomer. n
This diminution is directly related to the molar excluded volume per aggregate, B2.
Interaction leads to structural screening

## Slide 21
(174) Jouault, N.; Moll, J. F.; Meng, D.; Windsor, K.; Ramcharan, S.;
Kearney, C.; Kumar, S. K. Bound Polymer Layer in Nanocomposites. ACS Macro Lett. 2013, 2, 371−74.

## Slide 23
Yi C, Zhang S, Webb KT, Nie Z Anisotropic Self-Assembly of Hairy Inorganic Nanoparticles Accounts of Chem. Res. 50 12-21 (2017).
As σ exceeds the overlap threshold of chains, polymers are stretched from anchor points toward the solvent medium, entering the semidilute polymer brush (SDPB) regime. At even higher σ, the concentrated polymer brush (CPB) regime is accessed, which is featured by non-Gaussian chain characteristics and more extended chain conformations.

## Slide 24
(132) Rungta, A.; Natarajan, B.; Neely, T.; Dukes, D.; Schadler, L. S.; Benicewicz, B. C. Grafting Bimodal Polymer Brushes on Nanoparticles Using Controlled Radical Polymerization. Macromolecules 2012, 45, 9303−11.
Thermally dispersed particles
Diffusion is more efficient for smaller particles
Greater grafting density improves colloidal dispersion
Sheets
Chains
“Dispersed”
“Aggregates”

## Slide 25
Akcora P, Liu H, Kumar SK, Moll J, Li Y, Benicewicz BC, Schadler LS, Acehan D, Panagiotopoulos AZ, Pryamitsyn V, Ganesan V, Ilavsky J, Thiyagarajan P, Colby RH, Douglas JF Anisotropic self-assembly of spherical polymer-grafted nanoparticles Nat. Mat. 8 354-359 (2009).
Model:
Short-range attraction
de/kT fitting parameter (attraction)
Countered by entropy of distortion of grafted polymer chains
Entropy of distortion from coil-globule transition model

## Slide 26
The TEM data in Fig. 2a were taken from slices normal to the surfaces. We have taken 15 adjacent ≈100-nm-thick slices from a film with a matrix of M = 142kgmol−1, which show string-like morphologies in Fig. 2a, and find that the same ‘string- like’ structure is seen in each slice (see Supplementary Fig. S4b). Consequently, these objects are sheet-like. We have also analysed slices parallel to the casting surface and found qualitatively similar results (see Supplementary Fig. S4c). Evidently, these particles spontaneously assemble into sheets that are 2–5 particles (<100 nm) wide with lateral dimensions in the 1–10 μm range. A point to note here is that we see only hexagonal particle packings in the sheets (see Supplementary Fig. S5d). We do not see the other packings predicted by the theory/simulation.
106 kg/mole graft
Variable matrix
0.05 graft/nm2
5% silica
150°C
5-day 150°C annealing
Variable graft MW
And graft density
142 kg/mol matrix
5-day 150°C annealing
Variable graft MW
And graft density
42 kg/mol matrix
1st Row b
2nd Row b

## Slide 27
Akcora P, Liu H, Kumar SK, Moll J, Li Y, Benicewicz BC, Schadler LS, Acehan D, Panagiotopoulos AZ, Pryamitsyn V, Ganesan V, Ilavsky J, Thiyagarajan P, Colby RH, Douglas JF Anisotropic self-assembly of spherical polymer-grafted nanoparticles Nat. Mat. 8 354-359 (2009).
The USAXS gives the size of the primary particles, and also indicates the existence of larger scale mass fractal structures (with fractal dimension ~ 3). It is unclear why the particle sizes vary in the last three rows, while they remain relatively constant for the first three rows. We conjecture that this might represent local particle clustering. USAXS does not provide the dimensions of the large-scale clusters seen in the second row of Fig. 2b (samples with brush molecular mass of 34 and 106 kg/mol. respectively). This indicates that the cluster sizes are larger than 1 μm.
Fractal df ~ 1?
Fractal df ~ 1
Higher graft density
Lower graft density
Fractal of aggregates
df ~ 1
These are either correlated or screened
-4
-2
-1
-4
-2
-1

## Slide 28
Circle G”; Square G’
Filled = 5% Nanocomposite
Open = Polymer
Red = 142 kg/mole (Large Sheets)
Black = 42 kg/mole (Short Strings)
180°C
G’ ~ G” => Network
Steady Shear 0.1 s-1 180°C
Red open = 142 kg/mole Matrix
Red filled = Filled 106 kg/mole 0.05/nm2 (Large Sheets)
Black open = 42 kg/mole Matrix
Black filled = Filled 106 kg/mole 0.05/nm2 (Short Strings)
Blue = 142 kg/mole Filled 158kg/mole 0.01/nm2
42 kg/mole
142 kg/mole

## Slide 29
Kumar SK, Jouault N, Benicewicz B, Neely T Nanocomposites with Polymer Grafted Nanoparticles Macromolecules 46 3199-3214 (2013).

## Slide 31
-4
-2

## Slide 32
“Extent of Crowding”
s = surface coverage
N = Graft MW
N0.5 ~ Radius
Number/area * thickness
1/a = Matrix/Graft MW
0.1 short matrix MW
10 long matrix MW
Well Dispersed
Phase Separated
Sheets
Strings
Clusters
Kumar, S.K., Jouault, N., Benicewicz, B. and Neely, T., 2013. Nanocomposites with polymer grafted nanoparticles. Macromolecules, 46(9), pp.3199-3214.

## Slide 33
Akcora P, Liu H, Kumar SK, Moll J, Li Y, Benicewicz BC, Schadler LS, Acehan D, Panagiotopoulos AZ, Pryamitsyn V, Ganesan V, Ilavsky J, Thiyagarajan P, Colby RH, Douglas JF Anisotropic self-assembly of spherical polymer-grafted nanoparticles Nat. Mat. 8 354-359 (2009).

## Slide 35
D = kT/(6pRHh)
<x2> = 2Dt

## Slide 37
Agglomerated
Network
Sheets
Agglomerated
Network
Sheets

## Slide 39
Long graft
Short graft
a = graft/matrix MW

## Slide 41
He J, Liu Y, Babu T, Wei Z, Nie Z Self-assembly of inorganic nanoparticle vesicles and tubules driven by tethered linear block copolymers. J. Am. Chem. Soc. 134 11342−11345 (2012).

## Slide 42
Huang J, Zhou J, Liu M Interphase in Polymer Nanocomposites JACS Au 2 280-291 (2022).

## Slide 47
Bailey EJ, Winey KI Dynamics of polymer segments, polymer chains, and nanoparticles in polymer nanocomposite melts: A review Prog. Polym. Sci. 105 101242 (2020)

## Slide 60
SE = Stokes-Einstein