## Slide 1
Zimm model predicts
D = kT/x = kT/(6p hs b N1/2) ~ N-1/df
= N x = 6p hs b N3/2 = 6p hs b N3/df
h ~ N3/df -1 = N0.5 or 0.8
Zimm Model (Non-draining)
~ ~

## Slide 2
Dilute Solution Chain
Dynamics of the chain
Rouse Motion
Rouse model predicts relaxation time follows N2
D = kT/x = kTN/t follows D ~ kT/N
Predicts that the viscosity will follow N which is true for low molecular weights in the melt and for fully draining polymers in solution
Rouse Model

## Slide 3
Rouse Model
For L = ∞ You have a wave solution with no modes for d
d is the phase shift between beads
t is the relaxation time z/kspr
There are four unknowns and two equations; z, t, t , d
So, we can solve for a relationship between t and d
Debye used ma for heat capacity
Debye gets w = (k/m)1/2

## Slide 4
Cyclic Boundary Conditions:
NR values of phase shift
For NR = 10

## Slide 5
Free End Boundary Conditions:
NR values of phase shift
NR Rouse Modes of order “m”
For NR = 10

## Slide 6
The amplitude of the Rouse modes is given by:
The amplitude is independent of temperature because the free energy of a mode is proportional to kT and the modes are distributed by Boltzmann statistics
90% of the total mean-square end to end distance of the chain originates from the lowest order Rouse-modes so the chain can be often represented as an elastic dumbbell

## Slide 7
Rouse dynamics
(like a dumbell response)
Dumbbell
Rouse

## Slide 9
Some rules and approaches for complex constitutive parameters
Cox-Merz Rule time measurements are equivalent to frequency measurements. Complex viscosity and steady shear viscosity are equivalent measurements.
Kramers-Kronig Relation
Since there is a response function, m(t), from which all mechanical responses can be calculated, then the loss and storage moduli are related to each other through the Cauchy integral, P().

## Slide 12
Consider the creep compliance, J(t) because it is easier to model.
(Stress relaxation is easier to measure, G(t).)
Maxwell Model or Simple relaxor or Dumbell Model

## Slide 13
Debye Single Relaxation time “Relaxor”
For an oscillatory strain
=

## Slide 14
Maxwell Model

## Slide 15
Cole-Cole Plot as an indication of a simple Debye relaxor
Ju is the unrelaxed compliance
(x-a)2 + (y-b)2 = r2

## Slide 16
Shear compliance, J*(w), easy to calculate. Shear modulus, G*(w), easy to measure.

## Slide 17
In the terminal flow regime
In the terminal flow regime for the dynamic compliance
At long times, the Maxwell element is just viscous

## Slide 18
In the terminal flow regime/low frequency regime
In the terminal flow regime for the dynamic compliance

## Slide 19
Rouse
Newtonian

## Slide 20
Rouse
Modulus has units of energy per volume, MPa
Each mode of vibration, p, in the Rouse Model has
Larger p modes have smaller tp so larger p modes are relaxed when t = tp
When t = tp there are p unrelaxed modes composed of segments with kT energy
Each of these segments have N/p monomers of volume b3
For a volume fraction of monomers of f, the number of unrelaxed segments per volume is f/(b3N/p)
So, the storage modulus is G(tp) ~ kT (f/(b3N/p)
We know that tp = t0 (N/p)2 so p ~ (t0/tp)1/2N and
G(tp) ~ kT (f/(b3N/p) = (kT/b3)f(tp/t0)-1/2 and for time t = tp G(t) ~ (kT/b3)f(t/t0)-1/2
G’(w) ~ (kT/b3)f(wt0)1/2 ~ (kT/b3)f(wh0)1/2
For t0 < t < tR
G(t) ~ (kT/b3)f(t/t0)-1/2 exp(-t/tR)
For t0 < t

## Slide 21
G(t) ~ (kT/b3)f(t/t0)-1/2 exp(-t/tR)
For t0 < t
For w < 1/t0
Rouse

## Slide 22
For wtR << 1, low frequency Normal Viscoelastic Fluid
kT per monomer
For 1/tR << w << 1/t0, Rouse Range, Fluid acts like a gel (Winter-Chambon)
(Solution in the limit tRw >> 1)
Rouse

## Slide 23
For 1/t0 << w, High Frequency limit
No relaxation modes,
G’(w ) = kT f/b3
High-frequency saturation of G’
G” (w ) ~ w
This is Solid Behavior

## Slide 24
Winter HH, Chambon F, Analysis of Linear Viscoelasticity of a Crosslinking Polymer at the Gel Point J. Rheo. 30 367-382 (1986).
The Power-Law is not Restricted in Frequency Range
G’(T, ) = G” (T, ) = (p/2)1/2 S(T) n, 0 < < ∞
S(T) = (2/p)1/2 C aT 1/2bT
Experimentally n = ½ (same as Rouse at moderate w)

## Slide 25
Winter HH, Chambon F, Analysis of Linear Viscoelasticity of a Crosslinking Polymer at the Gel Point J. Rheo. 30 367-382 (1986).
Kramers and Kronig relationship must be followed for this equation
Solve for n (only positive values are physical)

## Slide 28
Newtonian
Flow
Entanglement
Reptation
Rouse
Behavior

## Slide 30
Reptation
-One-dimensional diffusion along the tube
-Relaxation time, treptation, is the time for the chain to diffuse a distance L ~ N by Rouse diffusion, D0 ~ 1/N
Compare: tRouse ~ N2
Compare: DRouse ~

## Slide 31
Reptation
-Consider a Maxwell model for the fluid
Where G0 is the plateau modulus, G0 ~ 3kT/Me
Experimental shows N3.4 due to tube renewal

## Slide 32
Stress Relaxation Modulus for Reptation
te = t0Ne2
Follows Rouse Relaxation
G(t) ~ G0(t/t0)-1/2
For t0 < t < te

## Slide 34
Normal Stress and Recoverable Shear Compliance

## Slide 37
If there are multiple relaxations like x(t) = x0 exp-(t/t)
Each with an amplitude DJl and a relaxation time tl.
In integral form. Here we use ln t as the argument since each relaxation is of exponential form.
The modulus function has a similar form but dramatically different values for t.
Relaxation Spectrum (Ströbl (2007) p. 242-245)

## Slide 38
Relaxation Spectrum (Ströbl (2007) p. 242-245)
d lnt = dt/t
Then the functional dependence of interest is:
tHG(t) vs. t
That is why we see plots like:
Qiao H, Zheng B, Zhong G, Li Z, Cardinaels R, Moldenaers P, Lamnawar K, Maazouz A, Liu C, Zhang H Understanding the Rheology of Polymer-Polymer Interfaces Covered with Janus Nanoparticles: Polymer Blends versus Particle Sandwiched Multilayers Macromolecules 56 647- 663 (2023)

## Slide 40
Newtonian
Flow
Entanglement
Reptation
Rouse
Behavior