## Slide 1: Graphene-based Polymer Bulk Heterojunction Solar Cells
Fei Yu and Vikram Kuppa
School of Energy, Environmental, Biological and Medical Engineering
College of Engineering and Applied Science
University of Cincinnati
APS March Meeting 2012, Boston

## Slide 2: Solar Energy In Development
Renewable
Potential for High coverage
Low emission

## Slide 3: A comparison
Inorganic solar cells
From 1941
High processing cost
Thickness in microns
Not flexible
25.0% for Si cells*
Organic solar cells
From 1954
Solution processible
100~300 nm thick
Flexible
6.1% for polymer BHJ cells**
* Green, Progress in Photovoltaics, 2009. 17(3): p. 183-189.
** Park et al., Nat. Photonics, 2009. 3(5): p. 297-U5.

## Slide 4: Solar Cell Parameters
JSC: Short-circuit current density
VOC: Open-circuit voltage
Pmax: Maximum output power
FF: Fill factor
Power conversion efficiency (PCE)
η =
Picture source: Deibel and Dyakonov, Reports on Progress in Physics, 2010. 73(9): p. 1-39

## Slide 5: Polymer solar cells
e-
Single-layer device
HOMO: Highest Occupied Molecular Orbital
LUMO: Lowest Unoccupied Molecular Orbital
Epolymer
HOMO
LUMO
hν
e-
h+
h+
Exciton
An external voltage is required
Recombination of free charge carriers
~0.3 eV energy is needed to dissociate excitons

## Slide 6
D-A interface
EDonor
HOMODonor
LUMODonor
h+
Bilayer Device
e-
h+
D-A interface facilitates exciton dissociation
hν
EAcceptor
HOMOAcceptor
LUMOAcceptor
e-
0.3eV
Exciton dissociation is energetically favorable
Exciton diffusion length(~10 nm)
D-A interfacial area is limited by device geometry
Electron transfer from donor(semiconducting polymer) to acceptor

## Slide 7: Bulk Heterojunction(BHJ) Solar Cells
(Picture source: Deibel and Dyakonov, Reports on Progress in Physics, 2010. 73(9): p. 1-39)
*Peet et al., Nature Materials, 2007. 6(7) : p. 497-500.
Nanoscale penetrating network
Much increased D-A interfacial area
Over 6% PCE for P3HT:PCBM BHJs*
D-A interface close to where exciton is generated

## Slide 8: Donor Acceptor
Picture source: http://www.mpip-mainz.mpg.de/~andrienk/conferences/DPG_2009/
P3HT
Fullerene(C60)
Castro Neto et al., Reviews of Modern Physics, 2009. 81(1): p. 109-162
PCBM
Conjugated polymer

## Slide 9: Factors Affecting BHJ Performance
Pictures source: Dennler, Scharber and Brabec, Adv. Mater. 2009, 21(13): p. 1323-1338.
* Padinger, Rittberger and Sariciftci, Adv. Funct. Mater., 2003. 13(1): p. 85-88.
Choice of solvent: polymer chain packing
Donor-acceptor ratio: domain size
Annealing conditions: reorganize polymer chains, crystallization
Other post-production treatments: DC voltage during annealing for ordered structure *
Choice of donor and acceptor materials: band gap and miscibility
Morphology Performance

## Slide 10: BHJ features
Polymer:Fullerene BHJ device
High interfacial area for exciton dissociation
Bicontinuous network for charge transport
50:50 w/w P3HT:PCBM for optimum performance
Increase P3HT ratio to capture more solar energy
P3HT
PCBM
Notes: The most widely studied material in polymer:fullerene device is…
For such device, optimal device performance is achieved at 50:50 P3HT:PCBM ratio.
Excitons only generate in P3HT phase, and PCBM is photo-inactive
The goal of our research is to…

## Slide 11: Pristine Graphene
OPVs with chemically modified graphenes were reported*
Excellent conductivity and high aspect ratio
Percolation paths at very low fraction
Scale bar=50nm
TEM image of pristine graphene flake
Dia.~550nm
t=0.35 nm
*Liu, Z. et al., Adv. Mater., 2008. 20(20),
Yu, D. et al., ACS Nano, 2010. 4(10), Yu, D. et al., J. Phys. Chem. Lett., 2011. 2(10).
Notes: No functional groups
Conductivity: 2400 S m-1 for graphite
0.021 S m-1 for GO
As a result, we are able to make active layer with more than…

## Slide 12
        P3HT(~90.99%)
        PCBM(~9%)
        Graphene(~0.01%)
+

The Active layer

## Slide 13: Device Fabrication
Patterned ITO as bottom electrode
PEDOT:PSS by spin coating
10:1 P3HT:PCBM(w/w) with graphene by spin coating
LiF and Aluminum
Cathode
Anode
Fabricated and annealed in N2

## Slide 14: Device Characterization
J-V characteristics

## Slide 15
Cell performance summary
Notes: Dramatically increased Jsc and efficiency
Evidence of efficient charge transfer
Reduced Voc
Low FF limit device efficiency

## Slide 16: Cell performance summary(cont.)

## Slide 17: Device Characterization(cont.)
External Quantum Efficiency(EQE)*
Morphological change
*Yu and Kuppa, App. Phy. Lett. (submitted)
Notes: One thing we should notice here is the change of peak shape, and it is related to morphological change when graphene is added

## Slide 18
Recombination mechanism
Device Characterization(cont.)
JSC ~ PIn α
* Pientka, M. et al., Nanotechnology, 2004. 15(1): p. 163-170.
α=1: monomolecular(geminate) recombination
α=0.5: bimolecular(non-geminate) recombination
greater bimolecular recombination
Notes: Generally Jsc increase with illumination intensity exponentially, and the scaling behavior is an indicate of recombination mechanism.
Monomolecular: mobility of one charge carrier is much larger than the other.

## Slide 19: Conclusions
Adding small fraction of graphene greatly enhances charge transport and leads to much better Jsc and 
Cells with more than 90% P3HT are viable
Introduction of graphene in active layer leads to change of morphology
Device physics change with increasing graphene fraction
*Yu and Kuppa, App. Phy. Lett. (submitted)

## Slide 20: Future Work
Better dispersed and oriented graphene via morphological control
Increase FF by reducing interfacial roughness
Stability and device encapsulation
FY and VKK thank UC and the URC for funding and support

## Slide 21: Thank you!