## Slide 1: Sizing a battery
Max Yan
PhD candidate
University of Sheffield
myan5@sheffield.ac.uk

## Slide 2: About me
MEng Chemical Engineering (4 year programme)
  Year abroad at University at Buffalo (SUNY)
CDT in Energy Storage and its Applications (PhD)
  http://www.energystorage-cdt.ac.uk/
Supervisor – Prof. Siddharth Patwardhan
  https://www.svplab.com/
Porous silicon anodes for lithium-ion batteries
  Magnesiothermic reduction of silica

## Slide 3: Part 1 – Terminology and calculations

## Slide 4: Sizing up a battery – basic parameters and calculations
Voltage (V), Current (A)
Parallel and series circuits
Capacity, energy (Ah, Wh)
C-rate (C)

## Slide 5: Sizing up a battery – voltage, current, power
Electrical Engineering parameter | Chemical Engineering equivalent parameter
Voltage (V) | Fluid pressure (kPa, psi)
Current (A) | Flowrate (m³/s)
Electrical power (W) | Mechanical, or pump power (W)

## Slide 6: Sizing up a battery – parallel and series circuits
In series circuit (S), output voltage increases, current stays the same
In parallel circuit (P), output current increases, voltage stays the same
Batteries have maximum safe operating voltage (and current)
  Approx. 3.6V for Li-ion
  1.2 - 1.5V for NiMH
Increase voltage and current by connecting in P and S
V
1.2V
1.2V
1.2V
A
V
0.1A
0.1A
0.1A
0.3A
0.3A
0.3A
1.2V

## Slide 7: Sizing up a battery - capacity
C = Charge, in coulombs
t = time, in seconds
I = Current, in coulombs/s (amps)
Capacity, measured in amp-hours (Ah)
1 Ah capacity can supply a current of 1 A for 1 hour

## Slide 8: Capacity vs energy
Negative voltage
No usable energy
Ground level
Positive voltage
Usable energy
Capacity
Elevation
Voltage

## Slide 9: Sizing up a battery - energy
V = Voltage (V)
I = Current (A)
Cap = Capacity (Ah)
t = time (s)
P = Power (W)
E = Energy content (Wh)
Hence, energy content = capacity x voltage
Units of energy content in a battery given in watt-hours
Capacity

## Slide 10: Sizing up a battery – C-rate
Rate of charging/discharging of a battery
Quoted as multiple of capacity of battery
For example: taking a 3 Ah battery
C-rate | Current (A) | Time taken (hrs)
1C | 3 | 1
0.5C | 1.5 | 2
0.1C | 0.3 | 10
0.01C | 0.03 | 100

## Slide 11: Problem 1 – Boiling the kettle
2 kW kettle
Takes approx. 45 sec to boil 1 cup of water (for tea)

## Slide 12: Problem 2 - charging your phone
3000 mAh (3 Ah) capacity (Samsung Galaxy S8)
Charger capable of supplying 2A
Charging time (nominated 0% to 100%) approx. 2 hour (0.5C)
Voltage: 5V

## Slide 13: Comparing energy storage devices
Luo, X., Wang, J., Dooner, M., Clarke, J., 2015. Appl. Energy.

## Slide 14: Comparing batteries
Tarascon, J.-M., Armand, M., 2001. Nature.

## Slide 15: Part 2 – Common battery types

## Slide 16: Useful notes
Electrons are negative – flow of electrons is from –ve electrode (anode) to +ve electrode (cathode)
In electronics, current flows from positive to negative – this is convention
In batteries, when you charge, you store energy (and electrons) in the anode
In this section, all equations are written so that forward reactions are spontaneous

## Slide 17: Useful notes - refresher
Spontaneous reactions determined from standard electrode potentials
The more positive the potential, the more likely it will (spontaneously) accept electrons
Reduction reactions

## Slide 18: Nickel metal hydride
Negative electrode:
Positive electrode:
Hydrogen ion shuttling back and forth
Nominal voltage of 1.2V
Alkaline electrolyte (KOH)
Notes: La, Nd, Ce, Pr. Ni, Co, Mn, Al.
Ti, V. Zr, Ni, Cr, Co, Fe, Mn

## Slide 19: Lead acid
Negative plate:
Positive plate:
Overall discharge reaction:
Battery nominal voltage 2V
Sulfuric acid electrolyte
Overcharging can cause water splitting
Measure state of charge by
  Measuring voltage,
  Gravimetric measurement of electrolyte
May, G.J., Davidson, A., Monahov, B., 2018. J. Energy Storage 15, 145–157.

## Slide 20: Edison battery
Negative electrode
Positive electrode
Alkaline electrolyte (KOH)
  Easy to handle, only susceptible to in air
1.4 V dropping to 1.2 V during discharge
Durable – can be cycled many times without degradation
Slow charge and discharge – better for constant power supply

## Slide 21: Part 3 – Lithium-ion battery

## Slide 22: Lithium-ion battery
Intercalation reactions occur
Lithium-ions move into material lattices
Lithium ions shuttle back and forth
Graphite stores lithium when fully charged
Cathode accepts lithium during discharge
Lithium highly reactive
  Requires absence of water or oxygen during manufacture and operation

## Slide 23: Calculating theoretical specific capacity (mAh/g)
Z = charge on lithium ion (+1)
= number of lithium ions
= Avogadro’s constant
= elementary charge of an electron
Graphite theoretical specific capacity:
371 mAh/g

## Slide 24: Lithium ion battery calculations
What is the minimum amount of lithium in your smartphone?
Smartphone battery capacity around 3000 mAh (3.0 Ah)
0.77g of lithium metal was required to make the battery, but no longer in elemental form in the battery.

## Slide 25: Cell configurations
Cylindrical cells are most efficient
Can be wound with high tension
Commonly made into 18650 (18 mm dia, 65 mm height)
AA batteries are 14500, not usually lithium ion

## Slide 26: Lithium ion batteries for EVs
Tesla Model S 85
  85 kWh battery pack
  18650 cell type
  6 cells per module, 16 modules
  74 in parallel
  7104 cells total
  360V
Nissan Leaf
  24 kWh battery
  Pouch-cell type
  4 cells per module, 48 modules
  32.5 Ah per cell
  192 pouch cells total
1 cell
1 module
1 cell
1 module

## Slide 27: Discharge characteristics
Capacity (and energy stored) is dependent on C-rate
Battery degrades after cycling
Discharge at 0.1C (bottom left)
6 charge cycles (bottom right)

## Slide 28: Discharge characteristics
Discharge curve shape is dependent on cathode material
Spinel and olivine
  Have robust structure
  Do not distort when intercalating
Layered structures
  Distort during intercalation
  Energy is lost when lithium forces into structure
  Sloping voltage profile
Liu, C., Neale, Z.G., Cao, G., 2016. Mater. Today.

## Slide 29: Part 4 – Silicon anodes

## Slide 30: Anode materials

## Slide 31: Calculating theoretical specific capacity (mAh/g)
z = charge on lithium ion (+1)
= number of lithium ions
= Avogadro’s constant
= elementary charge of an electron
Silicon theoretical specific capacity:
3571 mAh/g
Graphite = 371 mAh/g

## Slide 32: Silicon
Very high capacity
Low cyclability
Needs to be porous

## Slide 33: Making silicon
Non-porous: Carbothermal reduction
Porous: electrochemical etching of Si wafer
(1) J. Entwistle, A. Rennie and S. Patwardhan, J. Mater. Chem. A, 2018.
(2) Karbassian, F. Porous Silicon. In Porosity - Process, Technologies and Applications; 2018.

## Slide 34: Magnesiothermic reduction (MgTR)

## Slide 35: Magnesiothermic reduction
Mg
Grind
Heat at 650ºC, 6 hours

## Slide 36: Acid washing
Add HCl
Filter

## Slide 37: Drawbacks of MgTR
Sintering, loss of surface area
Presently not scalable
Needs improvement in sustainability
Scale bars: 1 μm

## Slide 38: Thermal control
Low ramp rates
Low temperatures
Salt – thermal sink
Two-step reduction
W. Luo, X. Wang, C. Meyers, N. Wannenmacher, W. Sirisaksoontorn, M. M. Lerner and X. Ji, Sci. Rep., 2013.
S. A. Martell, Y. Lai, E. Traver, J. MacInnis, D. D. Richards, S. MacQuarrie and M. Dasog, ACS Appl. Nano Mater., 2019.
Without NaCl
With NaCl

## Slide 39: Eutectic reduction
Reduction proceeds at 450ºC
Mg-Al eutectic is formed at 650ºC

## Slide 40: Stöber synthesis
500 ± 17 nm
Scale bar: 2 μm
Scale bar: 500 nm
Scale bar: 20 nm
20 ± 2 nm
75 ± 8 nm

## Slide 41: MgTR – 500 nm
Scale bar: 1 μm
450ºC
550ºC
650ºC
750ºC

## Slide 42: MgTR – 20 nm
Scale bar: 10 nm
Stöber silica (20nm) reduces at 450ºC

## Slide 43: MgTR – yields (wt% Si)
Fumed silica (7 nm) reduces at 380ºC
Fumed silica
Stöber silica
Fumed and Stöber

## Slide 44: Coin cell electrode preparation
Anode
Cathode
Separator
Binder
Conductive additive
Active material
Current collector

## Slide 45: Making the electrode
Mix with carbon, water and binder

## Slide 46: Drawdown variables
Binder content

## Slide 47: Drawdown variables
Water content
Binder content
Drawdown thickness
Drying schedule

## Slide 48: Preliminary cell data
Poor initial capacity
Poor cyclability
Chart: Cycle number
FS,Sy 25:75 wt% | 815.1743 | 563.9911 | 429.5373 | 319.1346 | 278.3734 | 247.7543 | 220.8056 | 197.3824 | 176.6638 | 160.0019 | 147.0105 | 136.9651 | 128.6101 | 121.3658 | 115.5704 | 110.2096 | 105.6216 | 101.5648 | 97.9909 | 94.7551 | 91.8574

## Slide 49: Ideal drawdown
Smooth (consistent thickness)
No aggregates ‘dragging’ across foil

## Slide 50: Coin cell assembly
2016 Coin cell
Punched electrode

## Slide 51: Cell data
Low wt% silicon are not electronically connected
Degradation seen in higher wt% silicon
Consumption of active material during SEI formation
58 wt% Si
49 wt% Si
34 wt% Si
32 wt% Si

## Slide 52: BFD, reaction stoichiometry
Desirable reaction:
Parasitic reaction:
Dissolution reactions:

## Slide 53: Process handles (variables)
Reactant molar ratios
Degree of mixing
Size of mixture (reaction mass)
Heating rate
Process times
1
2
3,4
5

## Slide 54: Measurable outputs
Experimental
  Yield
  Properties
  Performance
Modelling
  Operational cost
  Capital cost
  Payback time

## Slide 55: Conversion, selectivity, yield
Conversion x Selectivity = Yield

## Slide 56: Chem Eng approach to Chemistry
Quantify the process
Identify biggest bottlenecks at process level (Chem Eng)
Remove bottlenecks using innovations at molecular level (Chemistry)

## Slide 57
Acknowledgements: